Supporting information

Sustainable biocarbon/tung oil coatings with hydrophobic and UV-shielding properties for outdoor wood substrates

Laetitia Marrot 1*, Mariem Zouari 2,3, Matthew Schwarzkopf 2,3, David Brian DeVallance 4

1 FRISSBE, Slovenian National Building and Civil Engineering Institute (ZAG), 1000 Ljubljana, Slovenia; laetitia.marrot@zag.si (L.M.)

2 Innorenew CoE, Livade 6, 6310 Izola, Slovenia; mariem.zouari@innorenew.eu (M.Z.), matthew.schwarzkopf@innorenew.eu (M.S.)

3 Faculty of Mathematics Natural Sciences and Information Technologies, University of Primorska, Muzejski Trg 2, 6000 Koper, Slovenia

4 College of Science and Technology, Commonwealth University, 401 North Fairview Street, Lock Haven, PA 17745, United States; ddevallanc@lockhaven.edu (D.B.D.)

* Corresponding author: laetitia.marrot@zag.si, +38630775762; FRISSBE, Slovenian National Building and Civil Engineering Institute (ZAG), 1000, Ljubljana, Slovenia

This Supporting Information includes 4 tables and 2 figures in total.

Table S1 Average L* values of the coated wooden substrates with onsite weathering time

| L* values | Onsite weathering time (days) |
| --- | --- |
| Coating | 0 | 34 | 64* | 97 | 125 | 155 | 180 |
| Beech | ref | 72.1±6.0 | 61.2±0.1 | 68.9 | 60.8±0.6 | 57.9±0.4 | 57.4±1.8 | 53.9±0.4 |
|  | 0% BC | 73.6±0.4 | 62.9±0.3 | 57.8 | 56.3±0.8 | 52.8±1.0 | 50.2±0.7 | 49.6±0.4 |
|  | 5% BC | 48.3±0.0 | 41.0±0.3 | 24.3 | 26.7±0.6 | 27.2±0.8 | 26.4±0.7 | 26.5±0.9 |
|  | 10% BC | 26.1±0.7 | 25.7±0.1 | 25.4 | 27.4±0.3 | 27.5±1.0 | 26.6±0.4 | 27.1±0.4 |
|  | 20% BC | 24.4±0.7 | 23.3±0.2 | 19.5 | 19.7±0.5 | 21.2±0.1 | 21.4±1.3 | 22.4±0.6 |
| Oak | ref | 48.5±0.3 | 52.6±0.8 | 63.3 | 56.9±2.3 | 54.1±2.2 | 51.6±2.9 | 51.0±2.1 |
|  | 0% BC | 49.8±0.4 | 54.4±0.5 | 49.4 | 51.5±1.5 | 48.8±2.2 | 47.5±0.3 | 47.9±1.4 |
|  | 5% BC | 31.8±0.7 | 37.2±0.6 | 27.3 | 27.9±0.7 | 27.4±1.3 | 27.6±0.5 | 26.9±1.1 |
|  | 10% BC | 24.0±0.5 | 27.2±0.1 | 25.5 | 25.4±0.6 | 25.5±0.6 | 25.0±1.0 | 25.2±0.8 |
|  | 20% BC | 23.5±0.4 | 24.0±0.5 | 22.2 | 21.3±0.3 | 22.1±0.7 | 22.3±0.7 | 22.5±0.3 |
| *Values are the average of 3 measurements minimum except for 64 days (one measurement) |

Table S2 Average a* values of the coated wooden substrates with onsite weathering time

| a* values | Onsite weathering time (days) |
| --- | --- |
| Coating | 0 | 34 | 64* | 97 | 125 | 155 | 180 |
| Beech | ref | 6.7±0.6 | 6.1±0.1 | 5.6 | 2.1±0.1 | 1.8±0.3 | 1.4±0.4 | 1.6±0.3 |
|  | 0% BC | 9.7±0.2 | 11.2±0.2 | 12.9 | 7.2±0.4 | 2.8±0.2 | 3.3±0.0 | 2.8±0.4 |
|  | 5% BC | 7.0±0.1 | 8.6±0.2 | 1.2 | 1.3±0.1 | 1.1±0.1 | 1.1±0.1 | 0.9±0.1 |
|  | 10% BC | 1.3±0.2 | 2.2±0.0 | 2.9 | 2.2±0.2 | 1.9±0.1 | 1.5±0.1 | 1.5±0.1 |
|  | 20% BC | 0.6±0.3 | 0.7±0.1 | 0.0 | 0.3±0.1 | 0.5±0.1 | 0.3±0.1 | 0.3±0.0 |
| Oak | Ref | 6.5±0.1 | 6.6±0.2 | 4.9 | 2.8±0.3 | 1.9±0.2 | 1.8±0.4 | 1.8±0.3 |
|  | 0% BC | 11.0±0.3 | 10.3±0.4 | 10.2 | 7.4±0.7 | 5.6±0.1 | 4.1±0.7 | 3.3±0.4 |
|  | 5% BC | 7.0±0.3 | 7.6±0.3 | 2.9 | 2.6±0.4 | 2.0±0.2 | 1.7±0.1 | 1.3±0.0 |
|  | 10% BC | 2.0±0.4 | 3.2±0.2 | 2.8 | 2.2±0.2 | 1.6±0.3 | 1.2±0.1 | 1.2±0.2 |
|  | 20% BC | 0.7±0.1 | 0.9±0.2 | -0.1 | 0.0±0.0 | 0.1±0.0 | 0.1±0.0 | 0.1±0.1 |
| *Values are the average of 3 measurements minimum except for 64 days (one measurement) |

Table S3 Average b* values of the coated wooden substrates with onsite weathering time

| b* values | Onsite weathering time (days) |
| --- | --- |
| Coating | 0 | 34 | 64* | 97 | 125 | 155 | 180 |
| Beech | ref | 18.2±1.9 | 17.3±0.1 | 15.0 | 9.5±0.3 | 7.8±0.5 | 6.3±0.4 | 5.8±0.6 |
|  | 0% BC | 25.6±0.2 | 25.3±0.3 | 25.3 | 18.2±0.2 | 12.8±0.3 | 9.8±0.2 | 8.5±0.8 |
|  | 5% BC | 18.0±0.1 | 16.9±0.3 | 2.2 | 2.9±0.2 | 3.2±0.2 | 2.7±0.3 | 2.7±0.2 |
|  | 10% BC | 2.6±0.7 | 4.8±0.1 | 5.3 | 5.1±0.2 | 4.9±0.1 | 4.2±0.1 | 4.1±0.1 |
|  | 20% BC | 1.2±0.3 | 1.3±0.1 | -1.1 | 0.1±0.2 | 0.8±0.2 | 0.7±0.2 | 0.9±0.2 |
| Oak | Ref | 17.1±0.2 | 20.5±0.4 | 17.1 | 12.0±1.1 | 10.7±0.7 | 8.3±1.0 | 7.5±0.5 |
|  | 0% BC | 24.7±0.4 | 27.4±0.7 | 25.2 | 19.8±1.7 | 16.4±0.5 | 12.6±1.0 | 10.4±0.9 |
|  | 5% BC | 12.9±0.4 | 17.0±1.0 | 5.8 | 5.1±0.5 | 4.3±0.8 | 3.7±0.3 | 3.1±0.1 |
|  | 10% BC | 3.3±0.8 | 6.1±0.2 | 4.4 | 3.8±0.4 | 3.4±0.3 | 2.8±0.5 | 2.8±0.4 |
|  | 20% BC | 0.9±0.2 | 1.6±0.3 | -0.4 | -0.4±0.1 | 0.0±0.1 | -0.1±0.1 | 0.1±0.1 |
| *Values are the average of 3 measurements minimum except for 64 days (one measurement) |

Table S4 Δ E values of the coated wooden substrates with onsite weathering time Δ E values Onsite weathering time (days) Coating 0 34 64 97 125 155 180 Beech Ref 0.0 11.0 10.1 8.8* 22.8 23.3 26.4 0% BC 0.0 10.9 14.3 10.5* 25.8 28.0 30.0 5% BC 0.0 7.6* 0.2 21.3* 2.8 1.6 1.3 10% BC 0.0 2.4 3.4 1.7 2.2 1.5 1.2 20% BC 0.0 1.1 4.6 3.8 2.6 2.3 1.6 Oak Ref 0.0 5.3 8.2 10.3 12.4 14.7 15.4 0% BC 0.0 5.4 4.9 8.6 13.5 16.8 19.2 5% BC 0.0 6.8 7.1 15.9* 5.1 4.9 4.2 10% BC 0.0 4.5* 0.6 3.1 0.9 1.7 1.4 20% BC 0.0 0.9 1.1 3.5 0.9 1.0 0.8 *Aberrant values that were removed from Fig. 9

Figure S1 Pictures of non-weathered and weathered beech substrates uncoated (reference) and coated with 0, 5, 10 and 20% BC in tung oil, with increasing BC content from left to right. Figure in color online only.

Figure S2 Pictures of non-weathered and weathered oak substrates uncoated (reference) and coated with 0, 5, 10 and 20% BC in tung oil, with increasing BC content from left to right. Figure in color online only.

Beech

Beech

Figure S1

Oak

Oak

Figure S2