Supplement 1: Precursors` PSD (particle size distribution): mass a) cumulative distribution Q3 and b) distribution curve q*3, plotted on a logarithmic abscissa. Abbreviations: ASo - untreated aged sediment, AS - calcined aged sediment, FSo - untreated fresh sediment, FS - calcined fresh sediment, FA – fly ash, LS – ladle slag.

Supplement 2: SEM micrographs of the precursors: a) calcined AS, b) calcined FS, c) FA, d) LS. Abbreviations: AS - calcined aged sediment, FS - calcined fresh sediment, FA – fly ash, LS – ladle slag.

Supplement 3: Phase composition (I/M = Illite/Muscovite, am. cont. = amorphous content) of the Na or K based FS-AAMs and the precursors in ma% determined from XRD-patterns using the Rietveld refinement. Minerals below 1% are not stated. The corresponding agreement indices R profile and Goodness of fit (GOF) are stated to indicate the refinement validity. Abbreviations: ASo - untreated aged sediment, AS - calcined aged sediment, FSo - untreated fresh sediment, FS - calcined fresh sediment, FA – fly ash, LS – ladle slag.

|  | Na based AAMs | K based AAMs | Precursors |
| --- | --- | --- | --- |
| phase | FS + X % FA | FS + X % LS | FS + X % FA | FS + X % LS | ASo | AS | FSo | FS | FA | LS |
|  | 0 | 20 | 30 | 10 | 20 | 30 | 0 | 10 | 20 | 30 | 10 | 20 | 30 |  |  |  |  |  |  |
| Quartz | 16.5 | 13.8 | 12.3 | 14.6 | 14.8 | 13.3 | 16.0 | 14.1 | 11.2 | 10.1 | 13.8 | 13.5 | 13.4 | 26.4 | 26.6 | 22.6 | 24.6 | 4.1 | 14.9 |
| I/M | 22.0 | 20.0 | 19.8 | 21.1 | 18.9 | 14.6 | 19.8 | 19.0 | 16.8 | 17.6 | 19.2 | 20.0 | 20.1 | 16.5 | 13.0 | 15.9 | 13.8 |  |  |
| Feldspar | 11.2 | 13.5 | 11.1 | 11.3 | 7.9 | 8.1 | 12.9 | 13.0 | 15.1 | 15.7 | 9.6 | 8.8 | 8.5 | 13.2 | 16.0 | 10.3 | 16.4 | 11.8 |  |
| Calcite | 1.1 |  | 1.1 | 1.3 | 1.5 | 1.8 | 1.6 | 1.7 | 1.5 | 1.4 | 2.2 | 5.8 | 6.5 | 1.1 | 1.3 | 1.5 | 1.2 |  | 16.3 |
| Dolomite | 5.4 | 5.5 | 4.8 | 5.8 | 6.0 | 5.9 | 7.8 | 7.3 | 6.3 | 6.2 | 8.2 | 8.5 | 6.9 | 14.0 | 1.3 | 14.7 | 3.5 |  | 17.7 |
| Kaolinite |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.0 |  |  |  |  |  |
| Hornblende |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 9.6 |  |  |  |  |
| Na2CO3 | 1.7 | 1.5 | 1.6 | 1.5 | 1.4 | 1.5 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| MnCr2O4 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.7 |
| Ankerite |  |  |  |  |  |  |  |  |  |  |  |  | 2.5 |  |  |  |  |  |  |
| Brucite |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.4 |
| Coesite |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.7 |  |  |
| Mullite |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 4.7 |  |
| MgFeO4 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.0 |  |
| Gehlenite |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 1.5 |  |
| Larnite |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 7.1 |
| am. cont. | 41.5 | 44.3 | 48.9 | 43.0 | 47.5 | 52.5 | 41.3 | 44.5 | 48.8 | 48.7 | 45.7 | 41.8 | 40.9 | 27.0 | 32.1 | 34.4 | 37.9 | 75.6 | 38.0 |
| R-profile | 4.8 | 4.4 | 4.4 | 4.4 | 4.4 | 4.4 | 6.0 | 5.9 | 5.2 | 4.9 | 5.6 | 5.3 | 5.2 | 9.0 | 7.8 | 9.1 | 8.4 | 2.8 | 5.8 |
| GOF | 5.9 | 5.4 | 5.4 | 5.4 | 5.3 | 5.4 | 6.6 | 6.4 | 5.3 | 5.5 | 5.9 | 5.5 | 5.3 | 12.3 | 10.0 | 12.5 | 10.8 | 3.4 | 7.5 |

Supplement 4: FTIR spectra of the precursors. Abbreviations: AS - calcined aged sediment, FS - calcined fresh sediment, FA – fly ash, LS – ladle slag.

Supplement 5: Values of the geometrical densities (ρ) and three-day bending (σBS) and compressive (σCS) strengths of the prepared AAMs with their standard deviations. Abbreviations: AS - calcined aged sediment, FS - calcined fresh sediment, FA – fly ash, LS – ladle slag.

| AAM mixture | ρ [g×cm-3] | stdev [g×cm-3] | σBS [MPa] | stdev [MPa] | σCS [MPa] | stdev [MPa] |
| --- | --- | --- | --- | --- | --- | --- |
| Pure AS (Na) | 1.95 | 0.01 | 1.19 | 1.03 | 7.94 | 1.76 |
| AS-10FA (Na) | 1.91 | 0.01 | 0.41 | 0.71 | 9.61 | 2.36 |
| AS-20FA (Na) | 1.90 | 0.02 | 1.92 | 0.40 | 19.14 | 1.69 |
| AS-30FA (Na) | 1.90 | 0.03 | 4.25 | 0.28 | 30.66 | 3.46 |
| AS-10LS (Na) | 2.07 | 0.00 | 3.47 | 0.00 | 15.30 | 0.00 |
| AS-20LS (Na) | 2.05 | 0.01 | 5.42 | 1.12 | 24.96 | 1.22 |
| AS-30LS (Na) | 2.07 | 0.01 | 6.47 | 0.73 | 25.64 | 3.12 |
| Pure AS (K) | 2.10 | 0.02 | 0.05 | 0.09 | 15.83 | 3.21 |
| AS-10FA (K) | 2.07 | 0.03 | 0.00 | 0.00 | 22.42 | 4.11 |
| AS-20FA (K) | 2.03 | 0.04 | 0.66 | 1.14 | 25.66 | 3.79 |
| AS-30FA (K) | 2.03 | 0.01 | 0.53 | 0.92 | 31.16 | 6.69 |
| AS-10LS (K) | 2.08 | 0.01 | 2.78 | 2.55 | 18.20 | 1.41 |
| AS-20LS (K) | 2.12 | 0.00 | 1.66 | 1.47 | 22.55 | 2.32 |
| AS-30LS (K) | 2.13 | 0.01 | 2.49 | 2.22 | 27.12 | 2.65 |
| Pure FS (Na) | 1.78 | 0.03 | 3.14 | 0.29 | 21.30 | 2.75 |
| FS-20FA (Na) | 1.78 | 0.03 | 5.48 | 3.65 | 28.11 | 3.10 |
| FS-30FA (Na) | 1.75 | 0.04 | 6.59 | 3.54 | 32.18 | 6.97 |
| FS-10LS (Na) | 1.84 | 0.04 | 7.46 | 4.38 | 30.21 | 3.81 |
| FS-20LS (Na) | 1.90 | 0.00 | 7.28 | 0.00 | 29.33 | 0.00 |
| FS-30LS (Na) | 1.96 | 0.01 | 7.11 | 3.57 | 30.02 | 2.87 |
| Pure FS (K) | 2.08 | 0.04 | 8.80 | 3.35 | 21.89 | 1.02 |
| FS-10FA (K) | 2.03 | 0.06 | 8.12 | 2.32 | 26.27 | 3.01 |
| FS-20FA (K) | 2.05 | 0.03 | 12.04 | 4.72 | 26.03 | 2.81 |
| FS-30FA (K) | 2.04 | 0.02 | 14.55 | 1.64 | 28.02 | 4.10 |
| FS-10LS (K) | 2.10 | 0.04 | 11.37 | 4.77 | 23.19 | 0.94 |
| FS-20LS (K) | 2.09 | 0.03 | 6.72 | 0.17 | 29.21 | 3.04 |
| FS-30LS (K) | 2.08 | 0.03 | 8.11 | 2.20 | 30.45 | 4.58 |

Supplement 6: SEM micrographs of the uncoated polished FS-AAMs prepared using the pure sediment (a-c) or containing 30 ma% FA (d-f) or LS (g-h) and activated using Na-based solutions. Abbreviations: FS - calcined fresh sediment, FA – fly ash, LS – ladle slag.

Supplement 7: EDXS element maps of the main elements for the Na-activator AAMs: a) pure FS, b) 30 ma% FA, c) 30 ma% LS. Abbreviations: FS - calcined fresh sediment, FA – fly ash, LS – ladle slag.

Supplement 8: SEM micrograph of the uncoated polished Na-activator based FS-AAM with 30 ma% additional LS, showing cracks. White crosses mark locations visually estimated to contain activated gel and used to acquire EDXS spot measurements. Abbreviations: FS - calcined fresh sediment, FA – fly ash, LS – ladle slag.

Supplement 9: Occurrence of a) Si/Al atomic ratios and b) Ca/Si atomic ratios for EDXS point measurements of the uncoated polished FS-AAMs prepared using the pure sediment or containing 30 ma% FA or LS and activated using Na-based solutions. c) Atomic % of Na, Mg, Al, Si and Ca, determined by EDXS spot measurements of the uncoated, polished  FS-AAMs prepared using the pure sediment or containing 30 ma% FA or LS and activated using Na-based solutions. Abbreviations: FS - calcined fresh sediment, FA – fly ash, LS – ladle slag.

c)

| Mixture | Pure FS [at%] | 30 ma% FA [at%] | 30 ma% LS [at%] |
| --- | --- | --- | --- |
| Number | Na | Mg | Al | Si | Ca | Na | Mg | Al | Si | Ca | Na | Mg | Al | Si | Ca |
| 1 | 33.1 | 5.5 | 7.6 | 35.5 | 12.4 | 26.1 | 6.6 | 7.9 | 45.0 | 8.0 | 21.0 | 13.2 | 6.8 | 44.4 | 9.2 |
| 2 | 35.8 | 4.0 | 10.5 | 36.5 | 7.3 | 29.8 | 4.6 | 9.4 | 40.5 | 9.2 | 38.4 | 8.1 | 4.8 | 25.8 | 9.7 |
| 3 | 34.8 | 5.9 | 9.5 | 38.7 | 5.9 | 26.1 | 2.7 | 15.5 | 41.2 | 5.4 | 21.3 | 4.1 | 11.9 | 45.6 | 11.3 |
| 4 | 33.2 | 4.8 | 8.7 | 37.2 | 9.6 | 31.2 | 2.8 | 9.8 | 38.7 | 9.7 | 28.3 | 4.1 | 11.8 | 38.4 | 12.5 |
| 5 | 31.0 | 6.2 | 7.2 | 41.7 | 9.0 | 33.8 | 3.6 | 10.1 | 37.9 | 8.0 | 24.5 | 4.7 | 7.3 | 44.8 | 11.9 |
| 6 | 42.8 | 4.0 | 7.3 | 33.8 | 7.9 | 26.4 | 4.1 | 12.9 | 41.7 | 7.1 | 27.9 | 4.9 | 6.8 | 45.0 | 10.3 |
| 7 | 43.1 | 4.6 | 7.9 | 33.0 | 6.4 | 30.5 | 3.3 | 9.0 | 39.8 | 11.0 | 24.2 | 8.5 | 7.0 | 42.7 | 13.5 |
| 8 | 31.5 | 7.9 | 7.4 | 39.4 | 8.2 | 24.1 | 3.7 | 14.7 | 41.3 | 6.6 | 24.0 | 7.9 | 8.1 | 41.5 | 12.7 |
| 9 | 29.1 | 6.5 | 7.0 | 42.5 | 10.7 | 28.3 | 3.7 | 8.7 | 43.4 | 10.8 | 26.1 | 4.6 | 8.3 | 41.4 | 14.4 |
| 10 | 27.0 | 5.2 | 10.3 | 41.7 | 8.7 | 32.4 | 4.1 | 11.3 | 39.4 | 6.4 | 26.6 | 7.8 | 8.2 | 38.8 | 13.1 |
| 11 | 25.8 | 4.9 | 8.9 | 46.2 | 8.4 | 29.7 | 3.6 | 11.8 | 40.3 | 7.8 | 23.7 | 6.0 | 8.9 | 43.1 | 13.0 |
| 12 | 34.2 | 3.8 | 10.5 | 34.8 | 9.0 | 26.1 | 3.7 | 10.9 | 44.3 | 9.4 | 21.3 | 9.1 | 17.7 | 37.2 | 10.0 |
| 13 | 33.1 | 5.0 | 6.8 | 36.1 | 13.6 | 34.5 | 5.6 | 9.5 | 39.2 | 4.8 | 24.8 | 6.7 | 10.6 | 39.9 | 11.9 |
| 14 | 25.2 | 10.8 | 9.0 | 42.3 | 7.2 | 26.4 | 3.0 | 16.4 | 40.7 | 7.6 | 27.5 | 7.7 | 7.2 | 34.4 | 13.6 |
| 15 | 28.1 | 11.8 | 7.4 | 41.8 | 6.9 | 27.6 | 4.9 | 9.4 | 41.8 | 8.8 | 26.1 | 3.6 | 12.6 | 44.2 | 8.2 |
| 16 | 39.4 | 6.4 | 6.9 | 34.5 | 6.7 | 22.6 | 3.9 | 11.6 | 47.8 | 8.3 | 29.6 | 4.0 | 9.1 | 42.2 | 11.9 |
| 17 | 24.8 | 2.5 | 14.9 | 49.2 | 4.8 | 23.3 | 3.9 | 12.4 | 43.4 | 10.3 | 32.7 | 9.6 | 6.4 | 32.7 | 9.2 |
| 18 | 38.0 | 5.5 | 9.0 | 36.3 | 6.1 | 22.1 | 7.3 | 10.0 | 47.6 | 7.2 | 25.5 | 3.5 | 7.2 | 43.5 | 16.7 |
| 19 | 34.0 | 4.7 | 8.0 | 35.4 | 10.8 | 21.9 | 5.0 | 10.6 | 49.1 | 7.7 | 25.5 | 4.9 | 11.0 | 40.3 | 12.4 |
| 20 | 32.8 | 8.9 | 7.7 | 37.4 | 9.2 | 25.0 | 3.9 | 10.0 | 47.0 | 8.3 | 24.9 | 6.5 | 7.5 | 43.1 | 13.6 |
| 21 | 28.2 | 10.0 | 8.1 | 41.3 | 7.5 | 23.5 | 5.1 | 10.8 | 45.0 | 9.3 | 26.6 | 6.7 | 7.9 | 40.5 | 14.4 |
| 22 | 37.3 | 5.5 | 5.8 | 34.8 | 9.2 | 30.9 | 4.2 | 12.2 | 39.3 | 7.0 | 23.1 | 5.3 | 10.1 | 41.7 | 13.7 |
| 23 | 27.5 | 4.9 | 8.2 | 42.8 | 11.9 | 23.7 | 4.0 | 11.0 | 45.3 | 9.7 | 23.1 | 4.9 | 8.9 | 42.1 | 16.4 |
| 24 | 31.5 | 7.3 | 9.6 | 38.4 | 7.7 | 30.7 | 3.2 | 11.4 | 40.3 | 8.5 | 20.2 | 10.4 | 8.9 | 43.6 | 11.3 |
| 25 | 25.7 | 9.7 | 8.3 | 42.4 | 9.1 | 25.5 | 6.5 | 12.0 | 38.1 | 8.3 | 24.8 | 5.1 | 12.4 | 46.0 | 8.2 |
| 26 | 35.7 | 2.9 | 9.1 | 35.5 | 7.5 | 23.7 | 3.5 | 13.4 | 45.5 | 7.5 | 25.7 | 3.7 | 7.4 | 46.1 | 13.0 |
| 27 | 28.8 | 3.3 | 6.6 | 44.4 | 14.0 | 32.8 | 2.3 | 10.6 | 34.2 | 6.5 | 25.1 | 6.3 | 10.8 | 39.3 | 11.8 |
| 28 | 29.1 | 3.3 | 6.8 | 44.1 | 13.9 | 24.5 | 2.6 | 10.9 | 45.9 | 11.5 | 22.9 | 4.7 | 6.0 | 46.4 | 16.8 |
| 29 | 28.8 | 3.6 | 7.1 | 43.5 | 14.0 | 21.3 | 4.7 | 14.8 | 45.7 | 8.1 | 25.2 | 3.8 | 6.9 | 41.7 | 18.4 |
| 30 | 29.1 | 3.5 | 6.7 | 43.9 | 13.2 | 24.2 | 3.4 | 12.5 | 44.0 | 9.8 | 24.7 | 5.0 | 7.0 | 41.7 | 17.9 |
| 31 | 31.7 | 7.3 | 8.7 | 39.7 | 7.0 | 20.4 | 2.6 | 12.1 | 49.8 | 7.5 | 22.4 | 5.5 | 12.7 | 41.9 | 12.5 |
| 32 | 30.2 | 6.8 | 8.3 | 40.4 | 9.9 | 31.4 | 2.7 | 9.9 | 36.6 | 8.0 | 23.7 | 5.0 | 7.3 | 44.0 | 16.0 |
| 33 | 33.1 | 3.7 | 9.1 | 38.6 | 10.1 | 22.1 | 7.4 | 11.4 | 44.7 | 7.2 | 21.4 | 5.2 | 14.0 | 41.4 | 12.0 |
| 34 | 34.1 | 4.0 | 9.0 | 35.8 | 9.0 | 21.5 | 10.0 | 8.9 | 46.9 | 6.3 | 24.6 | 5.8 | 7.0 | 41.1 | 17.4 |
| 35 | 30.9 | 7.0 | 8.6 | 41.4 | 7.0 | 35.8 | 2.9 | 9.7 | 38.4 | 8.4 | 23.6 | 4.9 | 8.5 | 42.3 | 15.8 |
| 36 | 24.5 | 6.1 | 7.8 | 51.9 | 4.9 | 27.9 | 3.1 | 14.3 | 37.1 | 6.5 | 23.9 | 13.5 | 6.9 | 40.6 | 10.7 |
| 37 | 27.8 | 3.9 | 9.8 | 42.9 | 10.9 | 28.0 | 3.5 | 10.2 | 43.4 | 10.1 | 24.9 | 9.4 | 7.7 | 39.0 | 14.6 |
| 38 | 30.2 | 4.5 | 10.7 | 40.6 | 8.3 | 27.0 | 3.3 | 10.3 | 44.0 | 10.4 | 28.7 | 5.5 | 7.8 | 36.9 | 12.6 |
| 39 | 37.2 | 4.3 | 10.1 | 36.8 | 7.4 | 21.4 | 3.2 | 12.6 | 46.3 | 9.8 | 20.6 | 12.4 | 6.7 | 44.0 | 11.5 |
| 40 | 26.6 | 4.9 | 8.2 | 43.8 | 12.0 | 22.1 | 4.6 | 12.8 | 45.0 | 9.0 | 24.4 | 11.3 | 6.3 | 40.8 | 13.8 |
| 41 | 27.0 | 4.6 | 6.9 | 44.8 | 12.4 | 29.7 | 4.7 | 10.6 | 39.7 | 8.4 | 36.4 | 4.7 | 7.7 | 31.3 | 10.0 |
| 42 | 28.4 | 3.3 | 6.1 | 45.8 | 7.7 | 28.6 | 3.7 | 10.5 | 42.9 | 9.3 | 23.4 | 5.8 | 10.8 | 38.5 | 12.5 |
| 43 | 34.3 | 5.5 | 7.3 | 40.2 | 8.1 | 26.1 | 4.7 | 10.8 | 43.4 | 8.5 | 25.2 | 14.3 | 8.0 | 36.7 | 10.4 |
| 44 | 32.1 | 3.6 | 10.5 | 36.8 | 7.9 | 23.9 | 2.7 | 9.0 | 52.2 | 6.5 | 22.6 | 13.9 | 7.4 | 44.7 | 6.9 |
| 45 | 26.0 | 5.4 | 9.6 | 43.6 | 9.5 | 24.4 | 4.6 | 12.7 | 37.8 | 7.6 | 26.7 | 10.7 | 8.3 | 38.7 | 9.3 |
| 46 | 24.5 | 8.7 | 7.5 | 47.7 | 7.0 | 29.8 | 3.2 | 10.5 | 40.5 | 9.0 | 19.8 | 16.7 | 7.3 | 42.3 | 9.7 |
| 47 | 38.7 | 3.7 | 7.0 | 31.1 | 8.8 | 24.9 | 4.0 | 10.3 | 41.7 | 8.5 | 25.7 | 5.4 | 8.8 | 41.8 | 13.6 |
| 48 | 28.8 | 5.2 | 7.5 | 43.2 | 11.6 | 22.8 | 7.6 | 12.3 | 42.2 | 5.7 | 21.9 | 11.8 | 8.5 | 40.4 | 11.5 |
| 49 | 21.3 | 5.1 | 8.0 | 53.4 | 7.4 | 24.3 | 4.0 | 12.5 | 42.9 | 9.3 | 22.8 | 6.6 | 10.6 | 39.7 | 12.5 |
| 50 | 26.2 | 6.1 | 10.5 | 43.3 | 8.8 | 24.4 | 3.8 | 11.3 | 45.1 | 10.1 |  |  |  |  |  |
| 51 | 33.8 | 4.8 | 8.4 | 36.7 | 10.4 | 24.0 | 6.2 | 11.2 | 43.8 | 7.9 |  |  |  |  |  |
| 52 | 27.4 | 7.3 | 8.4 | 45.8 | 6.0 | 24.1 | 3.3 | 12.2 | 44.4 | 10.3 |  |  |  |  |  |
| 53 |  |  |  |  |  | 24.6 | 4.1 | 8.6 | 49.6 | 9.1 |  |  |  |  |  |
| 54 |  |  |  |  |  | 19.7 | 15.5 | 7.9 | 48.4 | 3.5 |  |  |  |  |  |
| 55 |  |  |  |  |  | 23.9 | 4.5 | 10.5 | 45.6 | 10.1 |  |  |  |  |  |
| 56 |  |  |  |  |  | 22.9 | 3.6 | 12.4 | 45.5 | 9.7 |  |  |  |  |  |
| 57 |  |  |  |  |  | 23.0 | 3.9 | 12.7 | 45.5 | 9.3 |  |  |  |  |  |
| 58 |  |  |  |  |  | 20.2 | 15.2 | 8.1 | 46.4 | 4.7 |  |  |  |  |  |
| 59 |  |  |  |  |  | 23.4 | 3.3 | 12.3 | 45.1 | 9.8 |  |  |  |  |  |

Supplement 10: SEM micrographs of the uncoated polished FS-AAMs prepared using the pure sediment (a-c) or containing 30 ma% FA (d-f) or LS (g-h) and activated using K-based solutions. Abbreviations: FS - calcined fresh sediment, FA – fly ash, LS – ladle slag.

Supplement 11: EDXS element maps of the main elements for the K-activated AAMs: a) pure FS, b) 30 ma% FA, c) 30 ma% LS. Abbreviations: FS - calcined fresh sediment, FA – fly ash, LS – ladle slag.

Supplement 12: SEM micrograph of the uncoated polished K-activator based FS-AAM with 30 ma% additional FA, showing cracks. White crosses mark locations visually estimated to contain activated gel and used to acquire EDXS spot measurements. Abbreviations: FS - calcined fresh sediment, FA – fly ash, LS – ladle slag.

Supplement 13: Occurrence of a) Si/Al atomic ratios and b) Ca/Si atomic ratios for EDXS point measurements of the uncoated polished FS-AAMs prepared using the pure sediment or containing 30 ma% FA or LS and activated using K-based solutions. c) Atomic % of Na, Mg, Al, Si and Ca, determined by EDXS spot measurements of the uncoated polished  FS-AAMs prepared using the pure sediment or containing 30 ma% FA or LS and activated using K-based solutions. Abbreviations: FS - calcined fresh sediment, FA – fly ash, LS – ladle slag.

c)

| Mixture | Pure FS [at%] | 30 ma% FA [at%] | 30 ma% LS [at%] |
| --- | --- | --- | --- |
| Number | K | Mg | Al | Si | Ca | K | Mg | Al | Si | Ca | K | Mg | Al | Si | Ca |
| 1 | 30.1 | 4.3 | 7.7 | 47.2 | 5.25 | 28.1 | 2.8 | 8.6 | 48.2 | 8.8 | 28.6 | 4.1 | 6.6 | 46.7 | 10.6 |
| 2 | 27.6 | 3.5 | 9.2 | 49.7 | 5.13 | 28.2 | 2.2 | 8.4 | 49.1 | 8.4 | 31.4 | 3.0 | 7.0 | 45.0 | 10.4 |
| 3 | 21.7 | 2.1 | 28.1 | 38.6 | 4.26 | 23.7 | 2.1 | 11.4 | 49.7 | 7.7 | 22.5 | 3.3 | 8.0 | 53.8 | 7.8 |
| 4 | 15.2 | 3.7 | 29.4 | 44.1 | 2.95 | 28.3 | 2.1 | 8.3 | 49.7 | 8.4 | 29.6 | 2.8 | 6.6 | 47.9 | 9.9 |
| 5 | 29.6 | 4.7 | 10.4 | 42.9 | 6.76 | 27.8 | 3.0 | 8.9 | 49.2 | 7.4 | 30.7 | 3.7 | 10.1 | 40.0 | 11.4 |
| 6 | 31.6 | 6.6 | 5.2 | 50.0 | 3.70 | 21.9 | 3.3 | 23.5 | 43.2 | 4.3 | 26.1 | 4.0 | 8.9 | 46.5 | 9.5 |
| 7 | 32.0 | 5.5 | 5.7 | 49.7 | 3.79 | 27.1 | 5.3 | 8.2 | 50.4 | 5.4 | 29.4 | 4.1 | 6.8 | 44.9 | 11.8 |
| 8 | 27.5 | 5.6 | 10.1 | 42.9 | 7.27 | 28.6 | 3.1 | 9.7 | 48.4 | 5.7 | 29.2 | 3.7 | 6.9 | 45.2 | 11.8 |
| 9 | 28.2 | 7.0 | 5.8 | 46.2 | 10.04 | 23.6 | 3.0 | 11.6 | 49.9 | 7.2 | 30.1 | 5.2 | 5.7 | 45.9 | 9.8 |
| 10 | 25.0 | 3.9 | 16.5 | 46.7 | 2.81 | 28.8 | 2.1 | 7.9 | 49.3 | 8.2 | 5.6 | 1.4 | 18.4 | 55.4 | 2.6 |
| 11 | 21.2 | 4.0 | 22.5 | 46.1 | 2.50 | 28.4 | 2.1 | 8.0 | 49.1 | 8.7 | 28.8 | 5.6 | 6.1 | 47.4 | 8.9 |
| 12 | 26.3 | 7.7 | 5.2 | 44.6 | 13.39 | 27.9 | 2.7 | 8.3 | 49.7 | 7.6 | 30.6 | 3.2 | 6.3 | 45.6 | 11.3 |
| 13 | 27.5 | 6.8 | 5.7 | 43.6 | 13.60 | 27.8 | 2.4 | 8.3 | 49.9 | 7.8 | 30.5 | 2.6 | 6.9 | 46.2 | 10.9 |
| 14 | 32.5 | 5.4 | 6.3 | 44.4 | 6.06 | 28.0 | 2.4 | 8.1 | 50.0 | 7.5 | 29.2 | 3.9 | 6.4 | 46.7 | 10.2 |
| 15 | 33.1 | 5.3 | 5.6 | 48.8 | 3.68 | 23.3 | 3.7 | 11.0 | 51.8 | 5.9 | 30.2 | 2.6 | 7.5 | 45.9 | 10.7 |
| 16 | 32.6 | 5.5 | 6.4 | 47.9 | 3.69 | 20.4 | 2.6 | 21.9 | 46.7 | 4.0 | 26.5 | 5.0 | 7.4 | 45.2 | 11.0 |
| 17 | 12.0 | 10.0 | 14.7 | 45.2 | 9.77 | 19.2 | 2.7 | 21.6 | 49.6 | 3.2 | 25.6 | 5.1 | 7.6 | 43.9 | 13.3 |
| 18 | 16.4 | 3.0 | 15.5 | 49.2 | 3.82 | 27.5 | 2.4 | 8.5 | 47.9 | 8.7 | 25.9 | 4.6 | 10.2 | 46.4 | 9.1 |
| 19 | 32.6 | 4.4 | 8.4 | 43.3 | 6.11 | 27.7 | 2.6 | 9.6 | 46.8 | 8.6 | 15.1 | 2.5 | 15.0 | 48.4 | 6.1 |
| 20 | 28.7 | 5.3 | 8.2 | 47.9 | 4.17 | 28.3 | 2.1 | 8.4 | 48.0 | 8.7 | 26.8 | 4.9 | 8.8 | 43.3 | 9.3 |
| 21 | 32.5 | 4.2 | 6.9 | 48.9 | 3.72 | 28.7 | 2.8 | 13.1 | 42.4 | 8.4 | 27.5 | 5.5 | 7.5 | 46.5 | 8.9 |
| 22 | 26.9 | 12.3 | 5.1 | 49.1 | 4.07 | 21.7 | 3.6 | 9.3 | 56.8 | 4.6 | 16.2 | 3.1 | 12.8 | 53.8 | 6.2 |
| 23 | 28.3 | 13.6 | 5.2 | 46.4 | 3.88 | 26.5 | 5.4 | 8.4 | 49.0 | 7.1 | 24.6 | 5.0 | 11.3 | 45.3 | 9.3 |
| 24 | 30.3 | 9.2 | 5.2 | 48.3 | 4.07 | 30.1 | 3.7 | 9.5 | 43.4 | 8.0 | 23.0 | 4.3 | 7.0 | 53.0 | 8.0 |
| 25 | 31.8 | 5.9 | 5.8 | 47.1 | 6.24 | 23.3 | 4.5 | 9.4 | 53.0 | 5.9 | 21.0 | 4.7 | 12.4 | 45.4 | 7.1 |
| 26 | 32.9 | 4.7 | 6.6 | 47.9 | 4.41 | 27.5 | 3.5 | 8.9 | 47.8 | 8.6 | 27.9 | 2.3 | 6.6 | 49.8 | 10.7 |
| 27 | 27.6 | 6.0 | 9.9 | 47.5 | 4.33 | 21.8 | 2.8 | 13.1 | 49.8 | 7.0 | 27.8 | 2.8 | 6.5 | 48.9 | 11.4 |
| 28 | 25.4 | 4.7 | 10.6 | 51.0 | 3.89 | 4.5 | 0.9 | 19.7 | 56.0 | 2.0 | 29.9 | 4.4 | 6.0 | 45.9 | 9.9 |
| 29 | 19.4 | 1.9 | 30.9 | 42.1 | 2.76 | 23.2 | 4.6 | 10.7 | 47.1 | 9.7 | 21.7 | 4.9 | 15.7 | 47.0 | 5.3 |
| 30 | 34.2 | 3.1 | 7.4 | 37.3 | 11.20 | 25.0 | 4.3 | 9.7 | 50.2 | 6.1 | 21.7 | 4.6 | 16.8 | 42.6 | 7.9 |
| 31 | 33.2 | 2.1 | 7.5 | 38.3 | 10.23 | 27.5 | 2.9 | 11.8 | 46.5 | 5.8 | 21.4 | 4.9 | 8.5 | 46.3 | 14.9 |
| 32 | 21.9 | 3.3 | 6.6 | 60.3 | 4.15 | 28.1 | 3.2 | 14.1 | 39.5 | 7.4 | 15.4 | 3.1 | 30.4 | 45.3 | 3.0 |
| 33 | 18.2 | 2.3 | 30.5 | 43.3 | 2.47 | 10.2 | 1.3 | 21.7 | 62.6 | 1.8 | 30.0 | 3.7 | 6.4 | 45.7 | 11.1 |
| 34 | 36.2 | 2.9 | 9.0 | 35.2 | 10.02 | 12.1 | 1.6 | 31.6 | 42.7 | 2.5 | 25.2 | 5.3 | 8.7 | 44.3 | 12.4 |
| 35 | 40.1 | 2.5 | 8.2 | 30.4 | 11.29 | 21.7 | 2.5 | 13.6 | 52.1 | 4.8 | 22.5 | 5.5 | 13.3 | 45.5 | 8.4 |
| 36 | 33.4 | 1.9 | 5.0 | 41.8 | 11.45 | 25.2 | 3.1 | 17.5 | 43.2 | 5.4 | 26.1 | 5.0 | 7.4 | 44.8 | 12.3 |
| 37 | 28.6 | 3.6 | 13.1 | 39.5 | 6.97 | 25.5 | 3.0 | 14.8 | 45.3 | 5.8 | 30.5 | 3.3 | 6.4 | 44.5 | 11.6 |
| 38 | 29.9 | 6.9 | 6.6 | 48.6 | 4.66 | 20.5 | 3.3 | 19.6 | 48.2 | 3.8 | 26.4 | 4.6 | 7.8 | 45.5 | 12.6 |
| 39 | 27.8 | 5.9 | 7.5 | 49.5 | 4.73 | 29.7 | 1.6 | 8.6 | 48.3 | 8.0 | 29.8 | 3.5 | 10.0 | 41.3 | 11.3 |
| 40 | 30.3 | 7.4 | 6.3 | 48.9 | 3.86 | 28.7 | 2.0 | 8.3 | 48.9 | 8.2 | 30.1 | 3.9 | 6.9 | 45.0 | 11.3 |
| 41 | 26.4 | 5.8 | 9.3 | 49.6 | 4.47 | 22.9 | 2.9 | 7.9 | 55.8 | 6.4 | 30.0 | 2.9 | 6.8 | 46.5 | 11.0 |
| 42 | 6.3 | 1.1 | 23.0 | 52.5 | 5.37 | 22.4 | 4.3 | 12.7 | 45.5 | 9.4 | 28.8 | 3.4 | 7.4 | 46.5 | 11.1 |
| 43 |  |  |  |  |  | 24.5 | 3.7 | 10.0 | 45.6 | 10.9 | 15.1 | 3.0 | 13.8 | 55.2 | 6.3 |
| 44 |  |  |  |  |  | 26.3 | 4.6 | 9.5 | 50.0 | 4.9 | 28.5 | 3.0 | 7.8 | 47.7 | 9.9 |
| 45 |  |  |  |  |  |  |  |  |  |  | 29.0 | 4.1 | 7.1 | 45.4 | 11.3 |
| 46 |  |  |  |  |  |  |  |  |  |  | 25.2 | 5.8 | 6.8 | 48.4 | 10.4 |
| 47 |  |  |  |  |  |  |  |  |  |  | 29.3 | 4.7 | 5.9 | 45.2 | 12.0 |
| 48 |  |  |  |  |  |  |  |  |  |  | 19.5 | 4.6 | 12.8 | 52.8 | 6.0 |
| 49 |  |  |  |  |  |  |  |  |  |  | 25.0 | 6.4 | 8.7 | 42.5 | 10.4 |
| 50 |  |  |  |  |  |  |  |  |  |  | 29.4 | 4.1 | 7.2 | 44.1 | 11.7 |
| 51 |  |  |  |  |  |  |  |  |  |  | 27.4 | 4.3 | 9.2 | 44.3 | 11.0 |
| 52 |  |  |  |  |  |  |  |  |  |  | 24.0 | 5.2 | 12.3 | 45.9 | 8.3 |
| 53 |  |  |  |  |  |  |  |  |  |  | 24.7 | 6.1 | 11.4 | 44.4 | 10.1 |
| 54 |  |  |  |  |  |  |  |  |  |  | 27.3 | 4.7 | 7.2 | 44.0 | 13.7 |
| 55 |  |  |  |  |  |  |  |  |  |  | 28.0 | 3.6 | 7.1 | 47.6 | 10.4 |