# Supplementary information

Use of the modified controlled atmosphere cone calorimeter for the assessment of fire effluents generated by burning wood under different ventilation  conditions

Fire Technology

F. Knez, M. Uršič, N.Knez, K. Peeters, M. Franko, P. Zidar

# Author information

## Affiliations

Slovenian National Building and Civil Engineering Institute, Dimičeva 12, 1000 Ljubljana, Slovenia

Friderik Knez, Matija Uršič, Nataša Knez

Innorenew CoE, Livade 6, 6310 Izola, Slovenia

Kelly Peeters

Anton Marušič Institute, University of Primorska, Muzejski trg 2, 6000 Koper, Slovenia

Kelly Peeters

University of Nova Gorica, Vipavska 13, 5000 Nova Gorica, Slovenia

Mladen Franko

Biotehniška fakulteta, University of Ljubljana, Jamnikarjeva 101, 1000 Ljubljana, Slovenia

Primož Zidar

## Corresponding author

Correspondance to Primož Zidar.

E-mail: primoz.zidar@bf.uni-lj.si Fax: 01 256 57 82

# Samples and conditioning

Table 1: Sample names

| Material type | Oxygen level | 21% | 15% | 10% |
| --- | --- | --- | --- | --- |
| Spruce | PI1, PI2, PI3 | PI4, PI5, PI6 | PI7, PI8, PI9 |
| Particle Board | PB1, PB2, PB3 | PB4, PB5, PB6 | PB7, PB8, PB9 |
| OSB | O1, O2, O3 | O4, O5, O6 | O7, O8, O9 |

Spruce samples were cut from a single board, made from locally sourced spruce Picea abies.

Particle board samples were cut from a single board, locally sourced.

Oriented strain board samples were cut from a single board, locally sourced.

Samples were kept at 23±2°C and 50±5% relative humidity for weeks before experiments took place.

Table 2: Sample details

|  | Starting weight (g) | Total mass loss (g) | Densityǂ (kg/m3) | Wood humidity (%) | Burning behaviour (time of ignition (s)) |
| --- | --- | --- | --- | --- | --- |
| PI1 | 81,70 | 68,1 | 442 | 13,5 | flaming (23) |
| PI2 | 94,90 | 76,4 | 510 | 13,3 | flaming (37) |
| PI3 | 73,50 | 59,3 | 394 | 13,4 | flaming (40) |
| PI4 | 93,50 | 73,4 | 501 | 12,4 | flaming (27) |
| PI5 | 90,95 | 70,1 | 487 | 13,5 | flaming (27) |
| PI6 | 92,51 | 72,9 | 502 | 12,1 | flaming (25) |
| PI7 | 85,04 | 67,2 | 508 | 13,5 | smouldering |
| PI8 | 84,75 | 65,6 | 451 | 13,3 | smouldering |
| PI9 | 79,70 | 53,4 | 419 | 13,2 | smouldering |
| PB1 | 140,96 | 91,2 | 750 |  | flaming (39) |
| PB2 | 139,36 | 75,6 | 750 |  | flaming (41) |
| PB3 | 139,91 | 77,6 | 750 |  | flaming (39) |
| PB4 | 140,93 | 77,2 | 750 |  | flaming (37) |
| PB5 | 138,66 | 67,2 | 750 |  | smouldering |
| PB6 | 141,44 | 74,1 | 750 |  | flaming (39) |
| PB7 | 138,02 | 69,5 | 750 |  | smouldering |
| PB8 | 139,11 | 67,0 | 750 |  | smouldering |
| PB9 | 138,90 | 66,3 | 750 |  | smouldering |
| O1 | 118,45 | 80,5 | 640 |  | flaming (24) |
| O2 | 123,98 | 83,7 | 640 |  | flaming (23) |
| O3 | 115,20 | 77,1 | 640 |  | flaming (25) |
| O4 | 123,07 | 84,1 | 640 |  | flaming (23) |
| O5 | 114,3 | 77,3 | 640 |  | flaming (23) |
| O6 | 121,07 | 82,6 | 640 |  | flaming (24) |
| O7 | 127,85 | 76,3 | 640 |  | smouldering |
| O8 | 113,63 | 69,7 | 640 |  | smouldering |
| O9 | 119,98 | 72,5 | 640 |  | smouldering |

ǂParticle board and OSB densities are nominal

# Chromatograms of samples

Figure 1: Chromatogram of PI1 acetonitrile extract.

Figure 2: Chromatogram of PI1 hexane extract.

Figure 3: Chromatogram of PI2 acetonitrile extract.

Figure 4: Chromatogram of PI2 hexane extract.

Figure 5: Chromatogram of PI3 acetonitrile extract.

Figure 6: Chromatogram of PI3 hexane extract.

Figure 7: Chromatogram of PI4 acetonitrile extract.

Figure 8: Chromatogram of PI4 hexane extract.

Figure 9: Chromatogram of PI5 acetonitrile extract.

Figure 10: Chromatogram of PI5 hexane extract.

Figure 11: Chromatogram of PI6 acetonitrile extract.

Figure 12: Chromatogram of PI6 hexane extract.

Figure 13: Chromatogram of PI7 acetonitrile extract.

Figure 14: Chromatogram of PI7 hexane extract.

Figure 15: Chromatogram of PI8 acetonitrile extract.

Figure 16: Chromatogram of PI8 hexane extract.

Figure 17: Chromatogram of PI9 acetonitrile extract.

Figure 18: Chromatogram of PI9 hexane extract.

Figure 19: Chromatogram of PB1 acetonitrile extract.

Figure 20: Chromatogram of PB1 hexane extract.

Figure 21: Chromatogram of PB2 acetonitrile extract.

Figure 22: Chromatogram of PB2 hexane extract.

Figure 23: Chromatogram of PB3 acetonitrile extract.

Figure 24: Chromatogram of PB3 hexane extract.

Figure 25: Chromatogram of PB4 acetonitrile extract.

Figure 26: Chromatogram of PB4 hexane extract.

Figure 27: Chromatogram of PB5 acetonitrile extract.

Figure 28: Chromatogram of PB5 hexane extract.

Figure 29: Chromatogram of PB6 acetonitrile extract.

Figure 30: Chromatogram of PB6 acetonitrile extract.

Figure 31: Chromatogram of PB7 acetonitrile extract.

Figure 32: Chromatogram of PB7 hexane extract.

Figure 33: Chromatogram of PB8 acetonitrile extract.

Figure 34: Chromatogram of PB8 hexane extract.

Figure 35: Chromatogram of PB9 acetonitrile extract.

Figure 36: Chromatogram of PB9 hexane extract.

Figure 37: Chromatogram of O1 acetonitrile extract.

Figure 38: Chromatogram of O1 hexane extract.

Figure 39: Chromatogram of O2 acetonitrile extract.

Figure 40: Chromatogram of O2 hexane extract.

Figure 41: Chromatogram of O3 acetonitrile extract.

Figure 42: Chromatogram of O3 hexane extract.

Figure 43: Chromatogram of O4 acetonitrile extract.

Figure 44: Chromatogram of O4 hexane extract.

Figure 45: Chromatogram of O5 acetonitrile extract.

Figure 46: Chromatogram of O5 hexane extract.

Figure 47: Chromatogram of O7 acetonitrile extract.

Figure 48: Chromatogram of O7 hexane extract.

.

Figure 49: Chromatogram of O8 acetonitrile extract.

Figure 50: Chromatogram of O8 hexane extract.

Figure 51: Chromatogram of O9 acetonitrile extract.

Figure 52: Chromatogram of O9 hexane extract.

# List of detected compounds

Table 3: List of identified compounds in acetonitrile extracts and approximate common retention times.

| # | Retention time (min) | Library/ID | CAS |
| --- | --- | --- | --- |
| 1 | 4,2 | 2-Cyclopenten-1-one | 000930-30-3 |
| 2 | 4,3 | Crotonic acid | 003724-65-0 |
| 3 | 4,5 | 2-Furanmethanol | 000098-00-0 |
| 4 | 5,0 | Sulfurous acid, diethyl ester | 000623-81-4 |
| 5 | 5,1 | Pentanoic acid | 000109-52-4 |
| 6 | 5,2 | Tiglic acid | 000080-59-1 |
| 7 | 5,3 | 2-Cyclopenten-1-one, 2-methyl- | 001120-73-6 |
| 8 | 5,4 | 2(3H)-Furanone, dihydro- | 000096-48-0 |
| 9 | 5,7 | Phenol | 000108-95-2 |
| 10 | 5,9 | 2H-Pyran-2-one | 000504-31-4 |
| 11 | 6,3 | 2-Cyclopenten-1-one, 3-methyl- | 002758-18-1 |
| 12 | 7,1 | (3E)-3-Penten-1-yne | 002206-23-7 |
| 13 | 7,4 | 2-Cyclopenten-1-one, 2-hydroxy-3-methyl- | 000080-71-7 |
| 14 | 7,8 | Phenol, 2-methyl- | 000095-48-7 |
| 15 | 7,8 | Cycloheptanone, 4-methyl-, (R)- | 013609-59-1 |
| 16 | 8,1 | Ethanone, 1-(1H-pyrrol-2-yl)- | 001072-83-9 |
| 17 | 8,2 | p-Cresol | 000106-44-5 |
| 18 | 8,4 | Phenol, 2-methoxy- | 000090-05-1 |
| 19 | 8,7 | 1,3-Propanediamine, N-methyl- | 006291-84-5 |
| 20 | 8,7 | Phenol, 2,6-dimethyl- | 000576-26-1 |
| 21 | 8,8 | Maltol | 000118-71-8 |
| 22 | 8,9 | 2-Cyclopenten-1-one, 3-ethyl-2-hydroxy- | 021835-01-8 |
| 23 | 9,2 | 2-ethyl-phenol | 000090-00-6 |
| 24 | 9,4 | Phenol, 2,4-dimethyl- | 000105-67-9 |
| 25 | 9,7 | Phenol, 3-ethyl- | 000620-17-7 |
| 26 | 9,7 | Phenol, 3,5-dimethyl- | 000108-68-9 |
| 27 | 10,0 | Creosol | 000093-51-6 |
| 28 | 10,2 | Catechol | 000120-80-9 |
| 29 | 10,7 | 1,4:3,6-Dianhydro-.alpha.-d-glucopyranose | 997060-51-0 |
| 30 | 10,8 | Phenol, 4-ethyl-3-methyl- | 001123-94-0 |
| 31 | 11,1 | Phenol, 2,4,5-trimethyl- | 000496-78-6 |
| 32 | 11,2 | 1,2-Benzenediol, 3-methyl- | 000488-17-5 |
| 33 | 11,2 | 1,2-Benzenediol, 4-methyl- | 000452-86-8 |
| 34 | 11,4 | Benzeneethanol, 2-methoxy- | 007417-18-7 |
| 35 | 11,5 | Benzenethiol, o-isopropyl-, | 006262-87-9 |
| 36 | 11,6 | 1H-Inden-1-one, 2,3-dihydro- | 000083-33-0 |
| 37 | 11,8 | Naphthalene, 2-methyl- | 000091-57-6 |
| 38 | 12,0 | 2-methoxy-4-vinyl-phenol | 007786-61-0 |
| 39 | 12,1 | 1-Methylindan-2-one | 035587-60-1 |
| 40 | 12,2 | Furan, 3-methyl-2-(3-methyl-2-butenyl)- | 015186-51-3 |
| 41 | 12,2 | 2-Butynedioic acid, di-2-propenyl ester | 014447-07-5 |
| 42 | 12,3 | 3-Phenyl-2-propyn-1-ol | 001504-58-1 |
| 43 | 12,4 | Chavicol | 000501-92-8 |
| 44 | 12,5 | Phenol, 2,6-dimethoxy- | 000091-10-1 |
| 45 | 12,6 | Phenol, 2-methoxy-3-(2-propenyl)- | 001941-12-4 |
| 46 | 12,7 | 2-Methoxy-4-(n-propyl)phenol | 002785-87-7 |
| 47 | 12,9 | 1,3,5-Triazine-2,4,6(1H,3H,5H)-trione, 1,3,5-trimethyl- | 000827-16-7 |
| 48 | 13,1 | 4-Ethylcatechol | 001124-39-6 |
| 49 | 13,2 | 4-Hydroxy-3-methoxybenzaldehyde | 000121-33-5 |
| 50 | 13,3 | trans-Isoeugenol | 005932-68-3 |
| 51 | 13,4 | Benzenepropanal, 2-oxo- | 056485-04-2 |
| 52 | 13,6 | 2-Methyl-5-hydroxybenzofuran | 006769-56-8 |
| 53 | 13,7 | Naphthalene, 2,7-dimethyl- | 000582-16-1 |
| 54 | 13,8 | 3,5-Dimethoxy-4-hydroxytoluene | 006638-05-7 |
| 55 | 14,2 | Cyclohepta[b]pyran, 2,7-dihydro- | 054031-38-8 |
| 56 | 14,5 | Ethanone, 1-(4-hydroxy-3-methoxyphenyl)- | 000498-02-2 |
| 57 | 14,8 | Benzoic acid, 4-hydroxy-3-methoxy-, methyl ester | 003943-74-6 |
| 58 | 14,9 | 3-Furancarboxylic acid, 5-ethyl-2,4-dimethyl-, methyl ester | 071041-32-2 |
| 59 | 15,0 | 2-Propanone, 1-(4-hydroxy-3-methoxyphenyl)- | 002503-46-0 |
| 60 | 15,4 | d-Gluco-heptulosan | 997238-39-5 |
| 61 | 16,0 | .beta.-D-Glucopyranose, 1,6-anhydro- | 000498-07-7 |
| 62 | 16,1 | 1-Naphthol, 3-methyl- | 013615-40-2 |
| 63 | 16,3 | 1,4-Benzenedicarboxaldehyde, 2-methyl- | 027587-17-3 |
| 64 | 16,6 | Benzenepropanol, 4-hydroxy-3-methoxy- | 002305-13-7 |
| 65 | 17,0 | Cyclotetradecane | 000295-17-0 |
| 66 | 17,1 | Phenol, 2,6-dimethoxy-4-(2-propenyl)- | 006627-88-9 |
| 67 | 17,5 | 8-Methoxy-[1,2,4]triazolo[4,3-a]pyridine-3-thiol | 997148-51-9 |
| 68 | 17,7 | 4-((1E)-3-Hydroxy-1-propenyl)-2-methoxyphenol | 997145-89-7 |
| 69 | 17,7 | 9H-Fluoren-9-on | 000486-25-9 |
| 70 | 17,8 | 2-[(E)-non-1-en-3,5,7-triynyl]furan | 997148-02-5 |
| 71 | 17,9 | Syringylacetone | 019037-58-2 |
| 72 | 18,2 | Z-8-Hexadecene | 997292-17-2 |
| 73 | 18,3 | Anthracene | 000120-12-7 |
| 74 | 18,3 | Phenanthrene | 000085-01-8 |
| 75 | 20,0 | n-Hexadecanoic acid | 000057-10-3 |
| 76 | 20,4 | Cyclopentadecane | 000295-48-7 |
| 77 | 20,4 | Phenanthrene, 2,3,4,4a,9,10-hexahydro-1,4a-dimethyl-7-(1-methylethyl)-, (S)- | 023963-77-1 |
| 78 | 20,6 | Benzoic acid, 3-methyl-2-nitro- | 005437-38-7 |
| 79 | 20,7 | Phenylethylene, 3'-methoxy-2,2'-dinitro- | 016990-40-2 |
| 80 | 21,2 | [14]Annulene, 1,6:8,13-bis(methano)-, syn | 085385-68-8 |
| 81 | 21,2 | (3aR,7aS)-7a-buta-2,3-dienyl-3a-methyl-1,2,3,4,6,7-hexahydroinden-5-one | 997220-28-3 |
| 82 | 21,4 | 1-(9-methyl-9H-fluoren-2-yl)ethanone oxime | 997336-36-6 |
| 83 | 21,6 | 10,18-Bisnorabieta-5,7,9(10),11,13-pentaene | 006566-19-4 |
| 84 | 21,8 | 9,12-Octadecadienoic acid (Z,Z)- | 000060-33-3 |
| 85 | 21,8 | 9-Octadecenoic acid, (E)- | 000112-79-8 |
| 86 | 22,0 | Octadecanoic acid | 000057-11-4 |
| 87 | 22,2 | 2,3,5-Trimethyl-phenanthrene | 003674-73-5 |
| 88 | 22,2 | Hexadecanamide | 000629-54-9 |
| 89 | 22,3 | 7-Ethyl-2-fluorenyl methyl ketone | 997333-79-6 |
| 90 | 22,3 | 1-Nonadecene | 018435-45-5 |
| 91 | 22,4 | Docosane | 000629-97-0 |
| 92 | 22,6 | (Z)-2,3-dihydro-1H-cylonona[def]biphenylene | 104642-23-1 |
| 93 | 22,6 | 3,6-Dichloro-cyclohexa-3,5-dien-1,2-diol, cyclic butylboronate | 997365-23-2 |
| 94 | 22,7 | [1,1'-Biphenyl]-4,4'-diol, 3,3'-dimethoxy- | 004433-09-4 |
| 95 | 22,8 | Retene | 000483-65-8 |
| 96 | 23,2 | 1,1,5,6-Tetramethyl-1,2,3,4-tetrahydronaphthalene | 031197-54-3 |
| 97 | 23,3 | 1-Octadecene | 000112-88-9 |
| 98 | 23,3 | Tricosane | 000638-67-5 |
| 99 | 23,6 | 1,2,4,4-Tetramethylcyclopentene | 065378-76-9 |
| 100 | 23,7 | Acetic acid, (4-hydroxy-3-methoxyphenyl)-, methyl ester | 015964-80-4 |
| 101 | 23,8 | Methyl dehydroabietate | 001235-74-1 |
| 102 | 23,9 | 9-Octadecenamide, (Z)- | 000301-02-0 |
| 103 | 24,1 | 6,6-Diphenyl-D5-2,4-pentadienylidene-1 | 055530-35-3 |
| 104 | 24,2 | Guanidine, N-[3-[(2-bromophenyl)amino]-1-propenyl]- | 997444-82-0 |
| 105 | 24,2 | Tetracosane | 000646-31-1 |
| 106 | 24,4 | Phenol, 4-[[2-(3,4-dimethoxyphenyl)ethylamino]methyl]-2-methoxy- | 997618-00-8 |
| 107 | 24,8 | Dehydroabietic acid | 001740-19-8 |
| 108 | 25,0 | Cyclohexadecane, 1,2-diethyl- | 997491-46-9 |
| 109 | 25,1 | Hexadecane | 000544-76-3 |
| 110 | 25,2 | 5-Chlorovaleric acid, octadecyl ester | 997809-37-1 |
| 111 | 25,4 | Bis(2-ethylhexyl) phthalate | 000117-81-7 |
| 112 | 25,6 | 2-(3-Bromophenyl)-4-(3-butenoxy)tetrahydropyran | 997592-89-1 |
| 113 | 25,7 | 4-(9-Acridinyl)-2-methylbenzeneamine | 035586-76-6 |
| 114 | 25,9 | 7-oxo-dehydroabietic acid, methyl ester | 017751-36-9 |
| 115 | 26,1 | Benz(a)anthracene, 7-(methoxymethyl)-12-methyl- | 013345-60-3 |
| 116 | 26,4 | 2,5-Furandione, 3-dodecyl- | 059426-46-9 |
| 117 | 26,5 | (E)-3,3'-Dimethoxy-4,4'-dihydroxystilbene | 007329-69-3 |
| 118 | 26,5 | N-(1,3-dimethyl-2-aza-9-fluorenylidene)-p-toluidine | 997555-34-5 |
| 119 | 26,7 | Muscone | 000541-91-3 |
| 120 | 27,2 | 4'-Methyl-3,4,5-trimethoxychalcone, (E)- | 940291-94-1 |
| 121 | 27,2 | 7.beta.-Hydroxydehydroepiandrosterone | 002487-48-1 |
| 122 | 27,4 | 13-Docosenamide, (Z)- | 000112-84-5 |
| 123 | 27,5 | 9-Octadecenamide, (Z)- | 000301-02-0 |
| 124 | 27,8 | Retinoic acid | 000302-79-4 |
| 125 | 28,4 | 3,4-Divanillyltetrahydrofuran | 034730-78-4 |
| 126 | 28,6 | 2,4,6-Triphenylphosphinine | 013497-36-4 |
| 127 | 29,2 | Phenol, 4,6-ditert-butyl-2-(4-hydroxybenzylidenamino)- | 997643-85-5 |
| 128 | 29,2 | 4-methoxy-2,5-dimethyl-phenol | 997076-30-3 |
| 129 | 29,4 | (1S,2S)-2-Isopropyl-1-phenylsulfanylmethylspiro[4.5]decan-6-one | 997615-43-4 |
| 130 | 29,8 | Stigmasta-3,5-diene | 004970-37-0 |

Table 4: List of identified compounds in hexane extracts and approximate common retention times.

| # | Retention Time (min) | Library/ID | CAS |
| --- | --- | --- | --- |
| 1 | 4,2 | 2-Pentanone, 4-hydroxy-4-methyl- | 000123-42-2 |
| 2 | 6,4 | Butanoic acid | 000107-92-6 |
| 3 | 8,1 | Phenol, 3-methyl- | 000108-39-4 |
| 4 | 8,4 | Anhydro - sugar | 000000-00-0 |
| 5 | 9,3 | Phenol, 2,4-dimethyl- | 000105-67-9 |
| 6 | 9,5 | Benzoic acid | 000065-85-0 |
| 7 | 9,6 | 3,5-Xylenol | 000108-68-9 |
| 8 | 10,0 | 1-Dodecene | 000112-41-4 |
| 9 | 10,4 | 1,4:3,6-Dianhydro-.alpha.-d-glucopyranose | 997060-51-0 |
| 10 | 10,7 | Phenol, 4-ethyl-3-methyl- | 001123-94-0 |
| 11 | 10,8 | 2,3-Anhydro-d-mannosan | 997060-48-2 |
| 12 | 11,1 | Phenol, 2-ethyl-6-methyl- | 001687-64-5 |
| 13 | 11,2 | Phenol, 2,4,6-trimethyl- | 000527-60-6 |
| 14 | 11,3 | Phenol, 2,3,5-trimethyl- | 000697-82-5 |
| 15 | 11,3 | Pyrazine, 2-methoxy-3-(1-methylethyl)- | 025773-40-4 |
| 16 | 11,5 | 1,2-Benzenediol, 4-methyl- | 000452-86-8 |
| 17 | 11,5 | Phenol, 2-(2-propenyl)- | 001745-81-9 |
| 18 | 11,9 | 2-methoxy-4-vinyl-phenol | 007786-61-0 |
| 19 | 12,1 | 2-Methylresorcinol, acetate | 997108-45-3 |
| 20 | 12,3 | Chavicol | 000501-92-8 |
| 21 | 12,4 | Phenol, 2,6-dimethoxy- | 000091-10-1 |
| 22 | 12,5 | Eugenol | 000097-53-0 |
| 23 | 12,6 | 1H-Indenol | 056631-57-3 |
| 24 | 12,7 | Phenol, 2-methoxy-4-propyl- | 002785-87-7 |
| 25 | 12,7 | 1,3,5-Triazine-2,4,6(1H,3H,5H)-trione, 1,3,5-trimethyl- | 000827-16-7 |
| 26 | 13,1 | 1-Tetradecene | 001120-36-1 |
| 27 | 13,1 | 4-Hydroxy-3-methoxybenzaldehyde | 000121-33-5 |
| 28 | 13,3 | Phenol, 2-methoxy-4-(1-propenyl)- | 000097-54-1 |
| 29 | 13,4 | 1H-Benzo[d]imidazole, 5-methoxy | 004887-80-3 |
| 30 | 13,7 | 2-Propen-1-one, 1-(2-ethenyl-1-cyclohexen-1-yl)- | 115692-08-5 |
| 31 | 13,8 | 3,5-Dimethoxy-4-hydroxytoluene | 006638-05-7 |
| 32 | 13,8 | 3-Buten-2-one, 4-(3-methylphenyl)- | 015753-84-1 |
| 33 | 13,9 | Phenol, 2-methoxy-4-(1-propenyl)-, (Z)- | 005912-86-7 |
| 34 | 14,0 | Benzo[b]thiophene, 2,5-dimethyl- | 016587-48-7 |
| 35 | 14,2 | (3Z)-3-Ethylidene-2-methyl-1-hexen-4-yne | 076003-39-9 |
| 36 | 14,4 | Ethanone, 1-(4-hydroxy-3-methoxyphenyl)- | 000498-02-2 |
| 37 | 14,6 | Naphthalene, 1,2,3,4-tetrahydro-1,1,6-trimethyl- | 000475-03-6 |
| 38 | 14,6 | 2,4-Di-tert-butylphenol | 000096-76-4 |
| 39 | 14,8 | Benzoic acid, 4-hydroxy-3-methoxy-, methyl ester | 003943-74-6 |
| 40 | 14,9 | 2-Propanone, 1-(4-hydroxy-3-methoxyphenyl)- | 002503-46-0 |
| 41 | 15,3 | Phenol, 4-ethenyl-2,6-dimethoxy- | 028343-22-8 |
| 42 | 15,4 | 2,2-Dimethyl-5-methoxyindan | 997136-72-0 |
| 43 | 15,6 | 1-Propanone, 1-(4-hydroxy-3-methoxyphenyl)- | 001835-14-9 |
| 44 | 15,8 | Cetene | 000629-73-2 |
| 45 | 15,8 | Phenol, 2,6-dimethoxy-4-(2-propenyl)- | 006627-88-9 |
| 46 | 15,9 | Phenol, 2-methoxy-4-(2-propenyl)-, acetate | 000093-28-7 |
| 47 | 16,4 | Benzenepropanol, 4-hydroxy-3-methoxy- | 002305-13-7 |
| 48 | 16,5 | 7H-Benzo[3,4]cyclobuta[1,2]cyclohepten-7-one, 6,8-dihydro- | 061765-30-8 |
| 49 | 17,0 | Cyclopentadecane | 000295-48-7 |
| 50 | 17,7 | 1,1'-Biphenyl, 2-nitro- | 000086-00-0 |
| 51 | 17,8 | Syringylacetone | 019037-58-2 |
| 52 | 17,8 | Benzene, 1,2-dimethyl-4-(phenylmethyl)- | 013540-56-2 |
| 53 | 18,2 | E-15-Heptadecenal | 997391-15-3 |
| 54 | 18,2 | Tetradecane | 000629-59-4 |
| 55 | 18,3 | Phenanthrene | 000085-01-8 |
| 56 | 19,3 | 1-Nonadecene | 018435-45-5 |
| 57 | 19,4 | Nonadecane | 000629-92-5 |
| 58 | 19,6 | Hexadecanoic acid, methyl ester | 000112-39-0 |
| 59 | 19,7 | Phenanthrene, 4-methyl- | 000832-64-4 |
| 60 | 20,2 | Cyclopropane carboxamide, 2-cyclopropyl-2-methyl-N-(1-cyclopropylethyl)- | 331416-19-4 |
| 61 | 20,4 | Cycloeicosane | 000296-56-0 |
| 62 | 20,4 | Phenanthrene, 2,3,4,4a,9,10-hexahydro-1,4a-dimethyl-7-(1-methylethyl)-, (S)- | 023963-77-1 |
| 63 | 20,8 | Phenanthrene, 3,6-dimethyl- | 001576-67-6 |
| 64 | 21,1 | di-p-Tolylacetylene | 002789-88-0 |
| 65 | 21,2 | Cyclotetradecane | 000295-17-0 |
| 66 | 21,3 | Cyclohexadecane | 000295-65-8 |
| 67 | 21,4 | Henicos-1-ene | 001599-68-4 |
| 68 | 21,4 | Heneicosane | 000629-94-7 |
| 69 | 21,5 | 9H-Fluorene, 9-butyl-9-methyl- | 042348-92-5 |
| 70 | 21,8 | cis-Vaccenic acid | 000506-17-2 |
| 71 | 21,9 | 10,18-Bisnorabieta-5,7,9(10),11,13-pentaene | 006566-19-4 |
| 72 | 22,0 | Palmitoleamide | 106010-22-4 |
| 73 | 22,2 | Hexadecanamide | 000629-54-9 |
| 74 | 22,2 | Dihydro - retene | 997333-97-3 |
| 75 | 22,3 | 1-[4-(2-p-Tolylvinyl)phenyl]ethanone | 997333-84-8 |
| 76 | 22,3 | 1-Docosene | 001599-67-3 |
| 77 | 22,4 | Docosane | 000629-97-0 |
| 78 | 22,8 | Retene | 000483-65-8 |
| 79 | 22,9 | 9-Tricosene, (Z)- | 027519-02-4 |
| 80 | 23,0 | (Z)-1-(1-Naphthyl)oct-3-en-1-yne | 997326-43-7 |
| 81 | 23,0 | Henicos-1-ene | 001599-68-4 |
| 82 | 23,2 | Benzenepropanoic acid, 3,5-bis(1,1-dimethylethyl)-4-hydroxy-, octadecyl ester | 002082-79-3 |
| 83 | 23,3 | Tricosane | 000638-67-5 |
| 84 | 23,8 | Methyl dehydroabietate | 001235-74-1 |
| 85 | 23,9 | 9-Octadecenamide, (Z)- | 000301-02-0 |
| 86 | 24,1 | Octadecanamide | 000124-26-5 |
| 87 | 24,2 | 1-Nonadecene | 018435-45-5 |
| 88 | 24,2 | Tetracosane | 000646-31-1 |
| 89 | 24,7 | methyl RO15 - dehydro - abietate (Mills cpd. XIXb) | 022465-60-7 |
| 90 | 24,7 | Docosane | 000629-97-0 |
| 91 | 24,9 | Octadecane, 1-(ethenyloxy)- | 000930-02-9 |
| 92 | 25,0 | 1-Docosene | 001599-67-3 |
| 93 | 25,1 | Eicosane | 000112-95-8 |
| 94 | 25,3 | Methyl 20-methyl-heneicosanoate | 997730-02-2 |
| 95 | 25,3 | Bis(2-ethylhexyl) phthalate | 000117-81-7 |
| 96 | 25,4 | Octadecane, 1-chloro- | 003386-33-2 |
| 97 | 25,8 | 1-Eicosene | 003452-07-1 |
| 98 | 25,9 | Octadecane | 000593-45-3 |
| 99 | 26,3 | 1-Tricosene | 018835-32-0 |
| 100 | 26,3 | 1-Tetracosene | 010192-32-2 |
| 101 | 26,4 | 1-Hexacosene | 018835-33-1 |
| 102 | 26,5 | Pentacosane | 000629-99-2 |
| 103 | 26,9 | Nonacos-1-ene | 018835-35-3 |
| 104 | 27,3 | 13-Docosenamide, (Z)- | 000112-84-5 |
| 105 | 27,4 | (E)-3-pentacosene | 997719-31-1 |
| 106 | 27,5 | Cyclohexane, (1-octylnonyl)- | 055124-77-1 |
| 107 | 28,2 | Nonacosane | 000630-03-5 |