## S1.1. Drying shrinkage

Similarly, with alkali-activated binders both samples experienced majority of the length change due to shrinkage in the first 7 days of reaction. The trend was stabilized between 28 and 60 days. Overall, WM mortars shrunk more in comparison to DM.

Fig. S1. Length change of the mortars during curing

## S1.2. Freeze-thaw

All DM and WM samples were freeze-thaw resistant after 150 cycles without damages on the corners or surfaces. Only changes observed was the change in color of the mortars after the tests.

Fig. S2. Before (soaked samples) and residual images of the mortars after exposure to freeze-thaw

## S1.3. SEM-EDX

Fig. S3. Elemental distribution of (a) DM and (b) Wm after 90 days.