Supplementary material

Article title: Evaluation of thermal conductivity estimation models with laboratory-measured thermal conductivities of sediments

Journal name: Environmental Earth Sciences

Authors: Simona Adrinek, Rao Martand Singh, Mitja Janža, Mateusz Żeruń, Grzegorz Ryżyński

Corresponding author: Simona Adrinek, Geological Survey of Slovenia, Dimičeva ulica 14, SI–1000 Ljubljana, Slovenia; simona.adrinek@geo-zs.si

Table 1 Values of non-cohesive sediment samples, measured in the laboratory.

| Sample | Sediment | Water content [%]* |  | Compaction* | Bulk density [g/cm3] | Porosity [%] | λb [W/m×K] |
| --- | --- | --- | --- | --- | --- | --- | --- |
| PNS-1A | Fine sand | D | <2,0 | C | 1,75 | 32,7 | 0,307 |
| PNS-1A |  | D | <2,0 | C | 1,75 | 32,7 | 0,307 |
| PNS-1A |  | D | <2,0 | C | 1,75 | 32,7 | 0,310 |
| PNS-1B |  | PS | 3,8 | C | 1,81 | 30,4 | 1,096 |
| PNS-1B |  | PS | 3,8 | C | 1,81 | 30,4 | 1,096 |
| PNS-1B |  | PS | 3,8 | C | 1,81 | 30,4 | 1,109 |
| PNS-1C |  | S | 21,0 | C | 1,97 | 24,2 | 2,875 |
| PNS-1C |  | S | 21,0 | C | 1,97 | 24,2 | 2,875 |
| PNS-1C |  | S | 21,0 | C | 1,97 | 24,2 | 2,927 |
| PNS-2A | Medium sand | D | <2,0 | C | 1,71 | 34,2 | 0,364 |
| PNS-2A |  | D | <2,0 | C | 1,71 | 34,2 | 0,363 |
| PNS-2A |  | D | <2,0 | C | 1,71 | 34,2 | 0,363 |
| PNS-2B |  | PS | 3,1 | C | 1,85 | 28,8 | 1,421 |
| PNS-2B |  | PS | 3,1 | C | 1,85 | 28,8 | 1,441 |
| PNS-2B |  | PS | 3,1 | C | 1,85 | 28,8 | 1,459 |
| PNS-2C |  | S | 17,1 | C | 2,15 | 17,3 | 2,996 |
| PNS-2C |  | S | 17,1 | C | 2,15 | 17,3 | 3,019 |
| PNS-2C |  | S | 17,1 | C | 2,15 | 17,3 | 3,010 |
| PNS-3s.A |  | D | <2,0 | L | 1,55 | 40,4 | 0,246 |
| PNS-3s.A |  | D | <2,0 | L | 1,55 | 40,4 | 0,246 |
| PNS-3s.A |  | D | <2,0 | L | 1,55 | 40,4 | 0,246 |
| PNS-3s.B |  | D | <2,0 | MC | 1,7 | 34,6 | 0,279 |
| PNS-3s.B |  | D | <2,0 | MC | 1,7 | 34,6 | 0,280 |
| PNS-3s.B |  | D | <2,0 | MC | 1,7 | 34,6 | 0,286 |
| PNS-3s.C |  | D | <2,0 | C | 1,85 | 28,8 | 0,335 |
| PNS-3s.C |  | D | <2,0 | C | 1,85 | 28,8 | 0,350 |
| PNS-3s.C |  | D | <2,0 | C | 1,85 | 28,8 | 0,351 |
| PNS-3wn.A |  | PS | 16,2 | L | 1,79 | 31,2 | 2,392 |
| PNS-3wn.A |  | PS | 16,2 | L | 1,79 | 31,2 | 2,406 |
| PNS-3wn.A |  | PS | 16,2 | L | 1,79 | 31,2 | 2,407 |
| PNS-3wn.B |  | PS | 14,1 | MC | 1,83 | 29,6 | 2,523 |
| PNS-3wn.B |  | PS | 14,1 | MC | 1,83 | 29,6 | 2,541 |
| PNS-3wn.B |  | PS | 14,1 | MC | 1,83 | 29,6 | 2,542 |
| PNS-3wn.C |  | PS | 12,7 | C | 1,87 | 28,1 | 2,630 |
| PNS-3wn.C |  | PS | 12,7 | C | 1,87 | 28,1 | 2,634 |
| PNS-3wn.C |  | PS | 12,7 | C | 1,87 | 28,1 | 2,640 |
| PNS-3psp.A |  | S | 24,0 | L | 1,84 | 29,2 | 2,822 |
| PNS-3psp.A |  | S | 24,0 | L | 1,84 | 29,2 | 2,826 |
| PNS-3psp.A |  | S | 24,0 | L | 1,84 | 29,2 | 2,827 |
| PNS-3psp.B |  | S | 20,2 | MC | 2,05 | 21,2 | 2,920 |
| PNS-3psp.B |  | S | 20,2 | MC | 2,05 | 21,2 | 3,013 |
| PNS-3psp.B |  | S | 20,2 | MC | 2,05 | 21,2 | 3,038 |
| PNS-3psp.C |  | S | 16,2 | C | 2,16 | 16,9 | 3,112 |
| PNS-3psp.C |  | S | 16,2 | C | 2,16 | 16,9 | 3,122 |
| PNS-3psp.C |  | S | 16,2 | C | 2,16 | 16,9 | 3,147 |
| PNS-4A | Coarse sand | D | <2,0 | C | 1,82 | 30,0 | 0,324 |
| PNS-4A |  | D | <2,0 | C | 1,82 | 30,0 | 0,324 |
| PNS-4A |  | D | <2,0 | C | 1,82 | 30,0 | 0,325 |
| PNS-4B |  | PS | 4,5 | C | 1,87 | 28,1 | 1,871 |
| PNS-4B |  | PS | 4,5 | C | 1,87 | 28,1 | 1,886 |
| PNS-4B |  | PS | 4,5 | C | 1,87 | 28,1 | 1,888 |
| PNS-4C |  | S | 17,6 | C | 1,98 | 23,8 | 2,732 |
| PNS-4C |  | S | 17,6 | C | 1,98 | 23,8 | 2,739 |
| PNS-4C |  | S | 17,6 | C | 1,98 | 23,8 | 2,715 |
| PNS-5A | Sand and gravel mix | D | <2,0 | C | 1,89 | 27,3 | 0,473 |
| PNS-5A |  | D | <2,0 | C | 1,89 | 27,3 | 0,474 |
| PNS-5A |  | D | <2,0 | C | 1,89 | 27,3 | 0,475 |
| PNS-5B |  | PS | 11,8 | C | 1,97 | 24,2 | 2,814 |
| PNS-5B |  | PS | 11,8 | C | 1,97 | 24,2 | 2,817 |
| PNS-5B |  | PS | 11,8 | C | 1,97 | 24,2 | 2,834 |
| PNS-5C |  | S | 14,1 | C | 2,22 | 14,6 | 3,277 |
| PNS-5C |  | S | 14,1 | C | 2,22 | 14,6 | 3,270 |
| PNS-5C |  | S | 14,1 | C | 2,22 | 14,6 | 3,293 |
| PNS-6A | Granule gravel | D | <2,0 | C | 1,68 | 35,4 | 0,229 |
| PNS-6A |  | D | <2,0 | C | 1,68 | 35,4 | 0,232 |
| PNS-6A |  | D | <2,0 | C | 1,68 | 35,4 | 0,234 |
| PNS-6B |  | PS | 5,4 | C | 1,73 | 33,5 | 1,878 |
| PNS-6B |  | PS | 5,4 | C | 1,73 | 33,5 | 1,826 |
| PNS-6B |  | PS | 5,4 | C | 1,73 | 33,5 | 1,827 |
| PNS-6C |  | S | 16,5 | C | 2,12 | 18,5 | 2,831 |
| PNS-6C |  | S | 16,5 | C | 2,12 | 18,5 | 2,866 |
| PNS-6C |  | S | 16,5 | C | 2,12 | 18,5 | 2,878 |

*D – dry, PS – partially saturated, S – saturated, L – loose, MC – medium compacted, C – compacted

Table 2 Values of cohesive sediment samples, measured in the laboratory.

| Sample | Sediment | Water content [%]* |  | Compaction* | Bulk density [g/cm3] | Porosity [%] | λb [W/m×K] |
| --- | --- | --- | --- | --- | --- | --- | --- |
| PS-1A | Silt | D | <2,0 | R | 1,79 | 31,3 | 0,809 |
| PS-1A |  | D | <2,0 | R | 1,79 | 31,3 | 0,828 |
| PS-1A |  | D | <2,0 | R | 1,79 | 31,3 | 0,833 |
| PS-1B |  | S | 27,0 | R | 2,11 | 18,7 | 2,139 |
| PS-1B |  | S | 27,0 | R | 2,11 | 18,7 | 2,141 |
| PS-1B |  | S | 27,0 | R | 2,11 | 18,7 | 2,143 |
| PS-1C |  | S | 27,0 | USS | 2,16 | 17,1 | 2,027 |
| PS-1C |  | S | 27,0 | USS | 2,16 | 17,1 | 2,028 |
| PS-1C |  | S | 27,0 | USS | 2,16 | 17,1 | 2,050 |
| PS-2A | Sandy loam/Glacial till | D | <2,0 | R | 1,93 | 25,7 | 1,141 |
| PS-2A |  | D | <2,0 | R | 1,93 | 25,7 | 1,145 |
| PS-2A |  | D | <2,0 | R | 1,93 | 25,7 | 1,145 |
| PS-2B |  | S | 18,3 | R | 2,15 | 17,3 | 2,547 |
| PS-2B |  | S | 18,3 | R | 2,15 | 17,3 | 2,564 |
| PS-2B |  | S | 18,3 | R | 2,15 | 17,3 | 2,586 |
| PS-3A |  | D | <2,0 | R | 2,01 | 22,9 | 1,421 |
| PS-3A |  | D | <2,0 | R | 2,01 | 22,9 | 1,423 |
| PS-3A |  | D | <2,0 | R | 2,01 | 22,9 | 1,475 |
| PS-3B |  | S | 13,7 | R | 2,18 | 16,0 | 2,566 |
| PS-3B |  | S | 13,7 | R | 2,18 | 16,0 | 2,571 |
| PS-3B |  | S | 13,7 | R | 2,18 | 16,0 | 2,578 |
| PS-4A |  | D | <2,0 | R | 1,97 | 24,4 | 1,266 |
| PS-4A |  | D | <2,0 | R | 1,97 | 24,4 | 1,270 |
| PS-4A |  | D | <2,0 | R | 1,97 | 24,4 | 1,283 |
| PS-4B |  | S | 16,8 | R | 2,12 | 18,6 | 2,298 |
| PS-4B |  | S | 16,8 | R | 2,12 | 18,6 | 2,298 |
| PS-4B |  | S | 16,8 | R | 2,12 | 18,6 | 2,308 |
| PS-5A | Glacial till | D | <2,0 | R | 1,98 | 23,8 | 1,112 |
| PS-5A |  | D | <2,0 | R | 1,98 | 23,8 | 1,117 |
| PS-5A |  | D | <2,0 | R | 1,98 | 23,8 | 1,129 |
| PS-5B |  | S | 16,4 | R | 2,11 | 18,9 | 2,065 |
| PS-5B |  | S | 16,4 | R | 2,11 | 18,9 | 2,107 |
| PS-5B |  | S | 16,4 | R | 2,11 | 18,9 | 2,111 |
| PS-6A | Clay | D | <2,0 | R | 1,71 | 34,2 | 0,744 |
| PS-6A |  | D | <2,0 | R | 1,71 | 34,2 | 0,749 |
| PS-6A |  | D | <2,0 | R | 1,71 | 34,2 | 0,746 |
| PS-6B |  | S | 22,9 | R | 2,10 | 19,2 | 1,861 |
| PS-6B |  | S | 22,9 | R | 2,10 | 19,2 | 1,875 |
| PS-6B |  | S | 22,9 | R | 2,10 | 19,2 | 1,880 |
| PS-6C |  | S | 38,0 | R | 1,90 | 26,9 | 1,359 |
| PS-6C |  | S | 38,0 | R | 1,90 | 26,9 | 1,367 |
| PS-6C |  | S | 38,0 | R | 1,90 | 26,9 | 1,382 |
| PS-6D |  | S | 51,2 | R | 1,72 | 34,0 | 1,061 |
| PS-6D |  | S | 51,2 | R | 1,72 | 34,0 | 1,089 |
| PS-6D |  | S | 51,2 | R | 1,72 | 34,0 | 1,092 |
| BIIV04 | Clay with gravels | S | 24,1 | USS | 2,01 | 22,7 | 1,770 |
| BIIV05 |  | S | 20,7 | USS | 2,01 | 22,7 | 1,770 |
| BIIV06A |  | S | 25,8 | USS | 2,00 | 23,1 | 1,750 |
| BIIV10 |  | S | 31,0 | USS | 1,92 | 26,2 | 1,630 |
| BIIV11 |  | S | 38,0 | USS | 1,86 | 28,5 | 1,370 |
| BIIV12 | Till with gravels | S | 16,6 | USS | 2,15 | 17,3 | 2,410 |
| BIIV13 | Clay with gravels | S | 25,6 | USS | 1,99 | 23,5 | 1,670 |
| BIIV14 |  | S | 28,6 | USS | 2,00 | 23,1 | 1,620 |
| BIIV15A | Clay | S | 27,5 | USS | 2,04 | 21,5 | 1,710 |
| BIIV19 | Loam with gravels | S | 14,4 | USS | 2,15 | 17,3 | 2,420 |
| BIIV20 | Silt | S | 14,9 | USS | 2,10 | 19,2 | 2,560 |
| BIIV23 | Clay | S | 22,9 | USS | 2,06 | 20,8 | 1,840 |
| BIIV27 | Loam with clay and gravels | S | 32,4 | USS | 1,48 | 43,1 | 1,480 |
| BIIV30 | Clay | S | 31,3 | USS | 1,60 | 38,5 | 1,600 |
| BIIV32 |  | S | 51,2 | USS | 1,08 | 58,5 | 1,080 |
| BIIV36 | Clay with fine sand | S | 41,0 | USS | 1,08 | 58,5 | 1,080 |
| BIIV37 | Silt with fine sand | S | 30,7 | USS | 1,48 | 43,1 | 1,480 |
| BIIV50 | Clay | S | 40,5 | USS | 1,28 | 50,8 | 1,280 |

*D – dry, S – saturated, USS – undisturbed sediment structure, R – recompacted

Table 3 Modelled results for non-cohesive sediment samples (GM – Geometric mean model, AM – Arithmetic mean model, HM – Harmonic mean model, C & K – Cote & Konrad model).

| Sample | Sediment | Measured λb | GM | AM | HM | Kersten | Kersten - modified | Johansen | C & K | C & K - modified |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PNS-1A | Fine sand | 2,875 | 0,868 | 0,495 | -0,108 | 1,089 | 0,718 | 0,492 | 1,220 | 1,095 |
| PNS-1A | Fine sand | 2,875 | 0,868 | 0,495 | -0,108 | 1,089 | 0,718 | 0,492 | 1,220 | 1,095 |
| PNS-1A | Fine sand | 2,927 | 0,876 | 0,498 | -0,107 | 1,089 | 0,718 | 0,492 | 1,220 | 1,095 |
| PNS-1B | Fine sand | 1,096 | 1,096 | 1,096 | 1,096 | 1,569 | 1,165 | 1,009 | 1,804 | 1,682 |
| PNS-1B | Fine sand | 1,096 | 1,096 | 1,096 | 1,096 | 1,569 | 1,165 | 1,009 | 1,804 | 1,682 |
| PNS-1B | Fine sand | 1,109 | 1,109 | 1,109 | 1,109 | 1,569 | 1,165 | 1,009 | 1,804 | 1,682 |
| PNS-1C | Fine sand | 0,307 | 1,331 | 2,736 | 0,104 | 3,243 | 2,735 | 3,404 | 2,915 | 2,965 |
| PNS-1C | Fine sand | 0,307 | 1,331 | 2,736 | 0,104 | 3,243 | 2,735 | 3,404 | 2,915 | 2,965 |
| PNS-1C | Fine sand | 0,310 | 1,355 | 2,788 | 0,104 | 3,243 | 2,735 | 3,404 | 2,915 | 2,965 |
| PNS-2A | Medium sand | 2,996 | 1,080 | 0,561 | -0,096 | 1,028 | 0,678 | 0,447 | 1,151 | 1,030 |
| PNS-2A | Medium sand | 3,019 | 1,077 | 0,560 | -0,096 | 1,028 | 0,678 | 0,447 | 1,151 | 1,030 |
| PNS-2A | Medium sand | 3,010 | 1,077 | 0,560 | -0,096 | 1,028 | 0,678 | 0,447 | 1,151 | 1,030 |
| PNS-2B | Medium sand | 1,421 | 1,421 | 1,421 | 1,443 | 1,529 | 1,101 | 1,015 | 1,924 | 1,794 |
| PNS-2B | Medium sand | 1,441 | 1,441 | 1,441 | 1,464 | 1,529 | 1,101 | 1,015 | 1,924 | 1,794 |
| PNS-2B | Medium sand | 1,459 | 1,459 | 1,459 | 1,482 | 1,529 | 1,101 | 1,015 | 1,924 | 1,794 |
| PNS-2C | Medium sand | 0,364 | 1,728 | 2,896 | 0,144 | 4,000 | 3,342 | 4,116 | 3,354 | 3,427 |
| PNS-2C | Medium sand | 0,363 | 1,742 | 2,919 | 0,144 | 4,000 | 3,342 | 4,116 | 3,354 | 3,427 |
| PNS-2C | Medium sand | 0,363 | 1,737 | 2,910 | 0,144 | 4,000 | 3,342 | 4,116 | 3,354 | 3,427 |
| PNS-3s.A | Medium sand | 2,822 | 0,888 | 0,478 | -0,088 | 0,817 | 0,539 | 0,312 | 0,920 | 0,817 |
| PNS-3s.A | Medium sand | 2,826 | 0,888 | 0,478 | -0,088 | 0,817 | 0,539 | 0,312 | 0,920 | 0,817 |
| PNS-3s.A | Medium sand | 2,827 | 0,888 | 0,478 | -0,088 | 0,817 | 0,539 | 0,312 | 0,920 | 0,817 |
| PNS-3s.B | Medium sand | 2,920 | 0,838 | 0,478 | -0,103 | 1,013 | 0,668 | 0,437 | 1,134 | 1,015 |
| PNS-3s.B | Medium sand | 3,013 | 0,841 | 0,479 | -0,103 | 1,013 | 0,668 | 0,437 | 1,134 | 1,015 |
| PNS-3s.B | Medium sand | 3,038 | 0,859 | 0,485 | -0,102 | 1,013 | 0,668 | 0,437 | 1,134 | 1,015 |
| PNS-3s.C | Medium sand | 3,112 | 0,838 | 0,501 | -0,124 | 1,257 | 0,829 | 0,628 | 1,415 | 1,281 |
| PNS-3s.C | Medium sand | 3,122 | 0,875 | 0,516 | -0,122 | 1,257 | 0,829 | 0,628 | 1,415 | 1,281 |
| PNS-3s.C | Medium sand | 3,147 | 0,878 | 0,517 | -0,122 | 1,257 | 0,829 | 0,628 | 1,415 | 1,281 |
| PNS-3wn.A | Medium sand | 2,392 | 2,392 | 2,300 | 0,399 | 2,353 | 1,960 | 2,236 | 2,290 | 2,283 |
| PNS-3wn.A | Medium sand | 2,406 | 2,406 | 2,314 | 0,400 | 2,353 | 1,960 | 2,236 | 2,290 | 2,283 |
| PNS-3wn.A | Medium sand | 2,407 | 2,407 | 2,315 | 0,400 | 2,353 | 1,960 | 2,236 | 2,290 | 2,283 |
| PNS-3wn.B | Medium sand | 2,523 | 2,523 | 2,431 | 0,416 | 2,408 | 1,992 | 2,308 | 2,416 | 2,402 |
| PNS-3wn.B | Medium sand | 2,541 | 2,541 | 2,449 | 0,416 | 2,408 | 1,992 | 2,308 | 2,416 | 2,402 |
| PNS-3wn.B | Medium sand | 2,542 | 2,542 | 2,450 | 0,416 | 2,408 | 1,992 | 2,308 | 2,416 | 2,402 |
| PNS-3wn.C | Medium sand | 2,630 | 2,630 | 2,529 | 0,424 | 2,486 | 2,045 | 2,460 | 2,596 | 2,580 |
| PNS-3wn.C | Medium sand | 2,634 | 2,634 | 2,533 | 0,424 | 2,486 | 2,045 | 2,460 | 2,596 | 2,580 |
| PNS-3wn.C | Medium sand | 2,640 | 2,640 | 2,539 | 0,424 | 2,486 | 2,045 | 2,460 | 2,596 | 2,580 |
| PNS-3psp.A | Medium sand | 0,246 | 1,115 | 2,654 | 0,087 | 2,773 | 2,351 | 2,981 | 2,633 | 2,670 |
| PNS-3psp.A | Medium sand | 0,246 | 1,116 | 2,658 | 0,087 | 2,773 | 2,351 | 2,981 | 2,633 | 2,670 |
| PNS-3psp.A | Medium sand | 0,246 | 1,117 | 2,659 | 0,087 | 2,773 | 2,351 | 2,981 | 2,633 | 2,670 |
| PNS-3psp.B | Medium sand | 0,279 | 1,491 | 2,798 | 0,118 | 3,604 | 3,034 | 3,739 | 3,097 | 3,161 |
| PNS-3psp.B | Medium sand | 0,280 | 1,538 | 2,891 | 0,118 | 3,604 | 3,034 | 3,739 | 3,097 | 3,161 |
| PNS-3psp.B | Medium sand | 0,286 | 1,551 | 2,916 | 0,119 | 3,604 | 3,034 | 3,739 | 3,097 | 3,161 |
| PNS-3psp.C | Medium sand | 0,335 | 1,817 | 3,015 | 0,147 | 4,008 | 3,340 | 4,127 | 3,384 | 3,456 |
| PNS-3psp.C | Medium sand | 0,350 | 1,823 | 3,025 | 0,147 | 4,008 | 3,340 | 4,127 | 3,384 | 3,456 |
| PNS-3psp.C | Medium sand | 0,351 | 1,838 | 3,050 | 0,147 | 4,008 | 3,340 | 4,127 | 3,384 | 3,456 |
| PNS-4A | Coarse sand | 2,732 | 0,841 | 0,497 | -0,119 | 1,204 | 0,794 | 0,583 | 1,322 | 1,209 |
| PNS-4A | Coarse sand | 2,739 | 0,841 | 0,497 | -0,119 | 1,204 | 0,794 | 0,583 | 1,322 | 1,209 |
| PNS-4A | Coarse sand | 2,715 | 0,843 | 0,498 | -0,119 | 1,204 | 0,794 | 0,583 | 1,322 | 1,209 |
| PNS-4B | Coarse sand | 1,871 | 1,871 | 1,859 | 0,787 | 1,813 | 1,373 | 1,320 | 2,047 | 1,960 |
| PNS-4B | Coarse sand | 1,886 | 1,886 | 1,874 | 0,789 | 1,813 | 1,373 | 1,320 | 2,047 | 1,960 |
| PNS-4B | Coarse sand | 1,888 | 1,888 | 1,876 | 0,790 | 1,813 | 1,373 | 1,320 | 2,047 | 1,960 |
| PNS-4C | Coarse sand | 0,324 | 1,280 | 2,595 | 0,105 | 3,157 | 2,641 | 3,309 | 2,972 | 2,996 |
| PNS-4C | Coarse sand | 0,324 | 1,284 | 2,602 | 0,105 | 3,157 | 2,641 | 3,309 | 2,972 | 2,996 |
| PNS-4C | Coarse sand | 0,325 | 1,272 | 2,578 | 0,105 | 3,157 | 2,641 | 3,309 | 2,972 | 2,996 |
| PNS-5A | Sand and gravel mix | 3,277 | 1,127 | 0,630 | -0,120 | 1,332 | 0,878 | 0,695 | 1,471 | 1,355 |
| PNS-5A | Sand and gravel mix | 3,270 | 1,129 | 0,631 | -0,120 | 1,332 | 0,878 | 0,695 | 1,471 | 1,355 |
| PNS-5A | Sand and gravel mix | 3,293 | 1,131 | 0,632 | -0,120 | 1,332 | 0,878 | 0,695 | 1,471 | 1,355 |
| PNS-5B | Sand and gravel mix | 2,814 | 2,814 | 2,718 | 0,477 | 2,816 | 2,308 | 2,964 | 2,848 | 2,858 |
| PNS-5B | Sand and gravel mix | 2,817 | 2,817 | 2,721 | 0,477 | 2,816 | 2,308 | 2,964 | 2,848 | 2,858 |
| PNS-5B | Sand and gravel mix | 2,834 | 2,834 | 2,738 | 0,477 | 2,816 | 2,308 | 2,964 | 2,848 | 2,858 |
| PNS-5C | Sand and gravel mix | 0,473 | 2,059 | 3,193 | 0,169 | 4,219 | 3,490 | 4,195 | 3,596 | 3,637 |
| PNS-5C | Sand and gravel mix | 0,474 | 2,055 | 3,186 | 0,169 | 4,219 | 3,490 | 4,195 | 3,596 | 3,637 |
| PNS-5C | Sand and gravel mix | 0,475 | 2,070 | 3,209 | 0,169 | 4,219 | 3,490 | 4,195 | 3,596 | 3,637 |
| PNS-6A | Granule gravel | 2,831 | 0,705 | 0,432 | -0,109 | 0,985 | 0,649 | 0,417 | 1,076 | 0,973 |
| PNS-6A | Granule gravel | 2,866 | 0,714 | 0,435 | -0,108 | 0,985 | 0,649 | 0,417 | 1,076 | 0,973 |
| PNS-6A | Granule gravel | 2,878 | 0,720 | 0,437 | -0,108 | 0,985 | 0,649 | 0,417 | 1,076 | 0,973 |
| PNS-6B | Granule gravel | 1,878 | 1,878 | 1,849 | 0,527 | 1,579 | 1,219 | 1,148 | 1,860 | 1,776 |
| PNS-6B | Granule gravel | 1,826 | 1,826 | 1,797 | 0,523 | 1,579 | 1,219 | 1,148 | 1,860 | 1,776 |
| PNS-6B | Granule gravel | 1,827 | 1,827 | 1,798 | 0,523 | 1,579 | 1,219 | 1,148 | 1,860 | 1,776 |
| PNS-6C | Granule gravel | 1,050 | 1,574 | 2,725 | 0,135 | 3,798 | 3,167 | 3,922 | 3,309 | 3,351 |
| PNS-6C | Granule gravel | 1,075 | 1,594 | 2,760 | 0,135 | 3,798 | 3,167 | 3,922 | 3,309 | 3,351 |
| PNS-6C | Granule gravel | 1,087 | 1,601 | 2,772 | 0,135 | 3,798 | 3,167 | 3,922 | 3,309 | 3,351 |

Table 4 Modelled results for cohesive sediment samples (GM – Geometric mean model, AM – Arithmetic mean model, HM – Harmonic mean model, C & K – Cote & Konrad model).).

| Sample | Sediment | Measured λb | GM | AM | HM | Kersten | Kersten - modified | Johansen | C & K | C & K - modified |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PS-1A | Silt | 2,027 | 2,190 | 0,989 | 2,027 | 0,134 | 0,864 | 0,340 | 0,885 | 0,849 |
| PS-1A | Silt | 2,028 | 2,242 | 1,008 | 2,028 | 0,134 | 0,864 | 0,340 | 0,885 | 0,849 |
| PS-1A | Silt | 2,050 | 2,255 | 1,013 | 2,050 | 0,134 | 0,864 | 0,340 | 0,885 | 0,849 |
| PS-1B | Silt | 2,139 | 1,179 | 2,031 | 0,809 | 3,272 | 2,795 | 2,809 | 1,827 | 1,965 |
| PS-1B | Silt | 2,141 | 1,180 | 2,033 | 0,828 | 3,272 | 2,795 | 2,809 | 1,827 | 1,965 |
| PS-1B | Silt | 2,143 | 1,181 | 2,035 | 0,833 | 3,272 | 2,795 | 2,809 | 1,827 | 1,965 |
| PS-1C | Silt | 0,809 | 1,178 | 1,929 | 0,809 | 3,485 | 2,977 | 2,942 | 1,848 | 2,007 |
| PS-1C | Silt | 0,828 | 1,179 | 1,930 | 0,828 | 3,485 | 2,977 | 2,942 | 1,848 | 2,007 |
| PS-1C | Silt | 0,833 | 1,192 | 1,952 | 0,833 | 3,485 | 2,977 | 2,942 | 1,848 | 2,007 |
| PS-2A | Sandy loam/Glacial till | 2,547 | 2,584 | 1,289 | 2,547 | 0,166 | 1,066 | 0,475 | 1,098 | 1,050 |
| PS-2A | Sandy loam/Glacial till | 2,564 | 2,593 | 1,293 | 2,564 | 0,166 | 1,066 | 0,475 | 1,098 | 1,050 |
| PS-2A | Sandy loam/Glacial till | 2,586 | 2,593 | 1,293 | 2,586 | 0,166 | 1,066 | 0,475 | 1,098 | 1,050 |
| PS-2B | Sandy loam/Glacial till | 1,141 | 1,470 | 2,447 | 1,141 | 2,974 | 2,581 | 2,666 | 1,923 | 2,029 |
| PS-2B | Sandy loam/Glacial till | 1,145 | 1,479 | 2,464 | 1,145 | 2,974 | 2,581 | 2,666 | 1,923 | 2,029 |
| PS-2B | Sandy loam/Glacial till | 1,145 | 1,492 | 2,486 | 1,145 | 2,974 | 2,581 | 2,666 | 1,923 | 2,029 |
| PS-3A | Sandy loam/Glacial till | 2,566 | 2,939 | 1,552 | 2,566 | 0,184 | 1,186 | 0,571 | 1,225 | 1,169 |
| PS-3A | Sandy loam/Glacial till | 2,571 | 2,943 | 1,554 | 2,571 | 0,184 | 1,186 | 0,571 | 1,225 | 1,169 |
| PS-3A | Sandy loam/Glacial till | 2,578 | 3,050 | 1,606 | 2,578 | 0,184 | 1,186 | 0,571 | 1,225 | 1,169 |
| PS-3B | Sandy loam/Glacial till | 1,421 | 1,544 | 2,474 | 1,421 | 2,749 | 2,423 | 2,581 | 2,003 | 2,086 |
| PS-3B | Sandy loam/Glacial till | 1,423 | 1,547 | 2,479 | 1,423 | 2,749 | 2,423 | 2,581 | 2,003 | 2,086 |
| PS-3B | Sandy loam/Glacial till | 1,475 | 1,552 | 2,486 | 1,475 | 2,749 | 2,423 | 2,581 | 2,003 | 2,086 |
| PS-4A | Sandy loam/Glacial till | 2,298 | 2,748 | 1,406 | 2,298 | 0,174 | 1,120 | 0,518 | 1,156 | 1,104 |
| PS-4A | Sandy loam/Glacial till | 2,298 | 2,757 | 1,410 | 2,298 | 0,174 | 1,120 | 0,518 | 1,156 | 1,104 |
| PS-4A | Sandy loam/Glacial till | 2,308 | 2,785 | 1,423 | 2,308 | 0,174 | 1,120 | 0,518 | 1,156 | 1,104 |
| PS-4B | Sandy loam/Glacial till | 1,266 | 1,272 | 2,191 | 1,266 | 2,727 | 2,377 | 2,504 | 1,926 | 2,005 |
| PS-4B | Sandy loam/Glacial till | 1,270 | 1,272 | 2,191 | 1,270 | 2,727 | 2,377 | 2,504 | 1,926 | 2,005 |
| PS-4B | Sandy loam/Glacial till | 1,283 | 1,278 | 2,201 | 1,283 | 2,727 | 2,377 | 2,504 | 1,926 | 2,005 |
| PS-5A | Glacial till | 2,065 | 2,373 | 1,249 | 2,065 | 0,178 | 1,143 | 0,536 | 1,180 | 1,127 |
| PS-5A | Glacial till | 2,107 | 2,383 | 1,254 | 2,107 | 0,178 | 1,143 | 0,536 | 1,180 | 1,127 |
| PS-5A | Glacial till | 2,111 | 2,409 | 1,266 | 2,111 | 0,178 | 1,143 | 0,536 | 1,180 | 1,127 |
| PS-5B | Glacial till | 1,112 | 1,134 | 1,957 | 1,112 | 2,674 | 2,334 | 2,469 | 1,928 | 2,002 |
| PS-5B | Glacial till | 1,117 | 1,157 | 1,999 | 1,117 | 2,674 | 2,334 | 2,469 | 1,928 | 2,002 |
| PS-5B | Glacial till | 1,129 | 1,160 | 2,003 | 1,129 | 2,674 | 2,334 | 2,469 | 1,928 | 2,002 |
| PS-6A | Clay | 1,061 | 2,208 | 0,941 | 1,861 | 0,121 | 0,776 | 0,290 | 0,687 | 0,656 |
| PS-6A | Clay | 1,089 | 2,223 | 0,946 | 1,875 | 0,121 | 0,776 | 0,290 | 0,687 | 0,656 |
| PS-6A | Clay | 1,092 | 2,214 | 0,943 | 1,880 | 0,121 | 0,776 | 0,290 | 0,687 | 0,656 |
| PS-6B | Clay | 1,861 | 1,010 | 1,751 | 0,744 | 3,024 | 2,599 | 2,006 | 1,383 | 1,496 |
| PS-6B | Clay | 1,875 | 1,018 | 1,765 | 0,749 | 3,024 | 2,599 | 2,006 | 1,383 | 1,496 |
| PS-6B | Clay | 1,880 | 1,021 | 1,770 | 0,746 | 3,024 | 2,599 | 2,006 | 1,383 | 1,496 |
| PS-6C | Clay | 1,359 | 0,578 | 1,204 | 0,744 | 2,707 | 2,287 | 1,902 | 1,271 | 1,369 |
| PS-6C | Clay | 1,367 | 0,581 | 1,212 | 0,749 | 2,707 | 2,287 | 1,902 | 1,271 | 1,369 |
| PS-6C | Clay | 1,382 | 0,587 | 1,227 | 0,746 | 2,707 | 2,287 | 1,902 | 1,271 | 1,369 |
| PS-6D | Clay | 0,744 | 0,360 | 0,865 | 0,744 | 2,276 | 1,908 | 1,755 | 1,188 | 1,266 |
| PS-6D | Clay | 0,749 | 0,370 | 0,893 | 0,749 | 2,276 | 1,908 | 1,755 | 1,188 | 1,266 |
| PS-6D | Clay | 0,746 | 0,371 | 0,896 | 0,746 | 2,276 | 1,908 | 1,755 | 1,188 | 1,266 |
| BIIV04 | Clay with gravels | 1,770 | / | / | 1,770 | 2,708 | 2,323 | 2,442 | 1,795 | 1,879 |
| BIIV05 | Clay with gravels | 1,770 | / | / | 1,770 | 2,554 | 2,205 | 2,344 | 1,825 | 1,891 |
| BIIV06A | Clay with gravels | 1,750 | / | / | 1,750 | 2,740 | 2,344 | 2,461 | 1,776 | 1,865 |
| BIIV10 | Clay with gravels | 1,630 | / | / | 1,630 | 2,604 | 2,214 | 2,370 | 1,698 | 1,781 |
| BIIV11 | Clay with gravels | 1,370 | / | / | 1,370 | 2,556 | 2,159 | 2,350 | 1,630 | 1,716 |
| BIIV12 | Till with gravels | 2,410 | / | / | 2,410 | 2,853 | 2,488 | 2,601 | 1,944 | 2,037 |
| BIIV13 | Clay with gravels | 1,670 | / | / | 1,670 | 2,691 | 2,303 | 2,428 | 1,772 | 1,856 |
| BIIV14 | Clay with gravels | 1,620 | / | / | 1,620 | 2,843 | 2,423 | 2,528 | 1,757 | 1,858 |
| BIIV15A | Clay | 1,710 | / | / | 1,710 | 2,967 | 2,532 | 1,985 | 1,345 | 1,455 |
| BIIV19 | Loam with gravels | 2,420 | / | / | 2,420 | 2,674 | 2,350 | 2,504 | 1,977 | 2,050 |
| BIIV20 | Silt | 2,560 | / | / | 2,560 | 2,531 | 2,220 | 2,380 | 1,943 | 2,001 |
| BIIV23 | Clay | 1,840 | / | / | 1,840 | 2,853 | 2,453 | 1,935 | 1,381 | 1,477 |
| BIIV27 | Loam with clay and gravels | 1,480 | / | / | 1,480 | 1,406 | 1,193 | 1,486 | 1,416 | 1,422 |
| BIIV30 | Clay | 1,600 | / | / | 1,600 | 1,650 | 1,403 | 1,374 | 1,223 | 1,240 |
| BIIV32 | Clay | 1,080 | / | / | 1,080 | 0,913 | 0,765 | 0,969 | 1,061 | 1,073 |
| BIIV36 | Clay with fine sand | 1,080 | / | / | 1,080 | 0,853 | 0,720 | 0,886 | 1,246 | 1,331 |
| BIIV37 | Silt with fine sand | 1,480 | / | / | 1,480 | 1,380 | 1,174 | 1,458 | 1,173 | 1,157 |
| BIIV50 | Clay | 1,280 | / | / | 1,280 | 1,134 | 0,956 | 1,094 | 1,151 | 1,171 |