# Supplementary information: Cement characterisation data

The particle size distribution was measured by a single, central laboratory using laser diffraction. Samples were dispersed in isopropanol and ultrasonicated before introduction into the measurement cell. Refractive index and absorbance were matched to the material appearance. The results are summarized in Table 1.

The chemical composition was measured by a single, central laboratory using X-ray fluorescence (XRF) spectrometry on fused beads. Loss on Ignition (LOI) was determined by measured mass loss after heating at 950 or 1050 °C for 2 hours. The results are presented in Table 8.

The phase composition was measured by three labs using quantitative X-ray powder diffraction (XRD) analysis. Two labs used CuKα radiation, one lab used CoKα radiation. Rietveld analysis of the collected data scans was used for quantitative analysis of phase fractions. The amorphous phase fraction was calculated by comparison to an external standard. The results are given in Table 9.

Table 1. Particle size volume distribution of the sample and reference cements. DV,x designates the particle size value corresponding to the Xth percentile in the cumulative volumetric particle size distribution.

| Sample | Dv,10 (μm) | Dv,50 (μm) | Dv,90 (μm) |
| --- | --- | --- | --- |
| PC Lab 1 | 1.0 | 8.8 | 38.8 |
| PC Lab 2 | 2.4 | 16.6 | 57.6 |

Table 2. Chemical composition in oxides (wt.%) of the reference cements.

| Oxides | PC Lab 1 | PC Lab 2 |
| --- | --- | --- |
| SiO2 | 19.76 | 20.03 |
| Al2O3 | 5.44 | 4.74 |
| TiO2 | 0.23 | 0.25 |
| MnO | 0.06 | 0.04 |
| Fe2O3 | 3.01 | 2.88 |
| CaO | 61.09 | 63.38 |
| MgO | 2.74 | 1.53 |
| K2O | 1.58 | 0.88 |
| Na2O | 0.15 | 0.15 |
| SO3 | 3.93 | 3.11 |
| P2O5 | 0.16 | 0.24 |
| LOI 950 °C | 1.20 | 2.71 |
| total XRF - 950 °C | 99.35 | 99.94 |
| LOI 1050 °C | - | - |
| total XRF - 1050 °C | - | - |

Table 3. Phase composition (wt.%) of the reference cements

| Phases | PC Lab 1 | PC Lab 2 |
| --- | --- | --- |
| C3S | 61.7 | 58.4 |
| C2S | 12.5 | 17.7 |
| C3A | 8.7 | 9.4 |
| C4AF | 6.4 | 2.3 |
| Portlandite |  | 3.4 |
| Periclase | 0.4 | 0.3 |
| Calcite | 8.9 | 5.5 |
| Gypsum |  | 1.7 |
| Anhydrite | 0.6 | 0.4 |
| Dolomite |  | 0.5 |
| Quartz | 0.8 | 0.3 |
| SUM | 100 | 99.9 |