Drava River sediment in clay brick production: characterization, properties, and environmental performance

Appendix A: Firing regime during pilot production process

Appendix B: Materials and processes included in the LCA study

| Inputs | TB | TB-SED | Transport distance (two-way) |
| --- | --- | --- | --- |
| Raw material |  |  |  |
| Clay | 474 kg | 238 kg | 5 km |
| Marl | 705 kg | 705 kg | 5 km |
| Expanded clay | 6.66 kg | 6.66 kg | 0 km |
| Sawdust | 5.91 kg | 5.91 kg | 30 km |
| Packaging |  |  |  |
| PE film | 0.467 kg | 0.467 kg | 240 km |
| PP film | 0.0102 kg | 0.0102 kg | 300 km |
| Wooden base | 0.0545 kg | 0.0545 kg | 70 km |
| Energy and water |  |  |  |
| Thermal energy – natural gas | 1350 MJ | 1350 MJ | / |
| Electricity | 160 MJ | 160 MJ | / |
| Diesel | 0.703 kg | 0.703 kg | / |
| Water | 118 kg | 118 kg | / |
| River sediment |  |  |  |
| Sediment | / | 236 kg | 500 km |
| Sediment processing – diesel fuel | / | 0.265 kg | / |
| In-situ disposal – avoided emissions |  |  |  |
| Zn | / | 1.27 ppb* | / |
| Cd | / | 0.03 ppb | / |
| Pb | / | 0.35 ppb | / |
| Outputs | Classic brick | Brick with sediment | Transport distance (two-way) |
| Emissions |  |  |  |
| CO2 emissions – carbonates release | 8.5 kg | 24.6 kg | / |

* ppb = parts per billion

Appendix C: The shrinkage and water absorption depending on the firing temperature for samples G0 (pure clay), G1-G3 (clay with Sed10) and G5-G8 (clay with Sed1)

| G0 |  |  |  | G1 |  |  | G2 |  |  | G3 |  |  | G5 |  |  | G6 |  |  | G7 |  |  | G8 |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| T (°C) | Shr. (%) |  | Wat. abs. (%) | T (°C) | Shr. (%) | Wat. abs. (%) | T (°C) | Shr. (%) | Wat. abs. (%) | T (°C) | Shr. (%) | Wat. abs. (%) | T (°C) | Shr. (%) | Wat. abs. (%) | T (°C) | Shr. (%) | Wat. abs. (%) | T (°C) | Shr. (%) | Wat. abs. (%) | T (°C) | Shr. (%) | Wat. abs. (%) |
| 775 | -1.1 |  | 15.9 | 777 | -0.5 | 16.8 | 785 | -0.5 | 17.9 | 785 | -0.4 | 19.3 | 772 | -0.3 | 17.5 | 772 | -0.4 | 19.3 | 771 | -0.3 | 20.2 | 771 | -0.1 | 23.6 |
| 822 | -0.5 |  | 15.9 | 823 | -0.4 | 16.6 | 828 | -0.3 | 17.3 | 828 | -0.4 | 19.0 | 821 | -0.2 | 17.1 | 821 | -0.3 | 18.7 | 820 | -0.7 | 19.6 | 820 | -0.3 | 23.4 |
| 873 | 0 |  | 14.6 | 875 | -0.3 | 15.5 | 878 | -0.1 | 16.9 | 878 | -0.5 | 18.6 | 872 | 0.2 | 16.4 | 872 | -0.2 | 18.1 | 871 | -0.2 | 18.8 | 871 | -0.7 | 25.2 |
| 918 | 0.1 |  | 13.4 | 920 | 0.2 | 14.3 | 922 | 0.2 | 16 | 922 | 0.1 | 18.2 | 916 | 0.5 | 15.7 | 916 | 0.3 | 17.8 | 915 | 0.0 | 20.0 | 951 | -0.2 | 25.0 |
| 969 | 1.6 |  | 11.9 | 970 | 0.8 | 13.2 | 971 | 0.4 | 15.5 | 971 | 0.1 | 18.2 | 968 | 0.4 | 15.1 | 968 | -0.2 | 17.9 | 968 | 0.2 | 20.1 | 968 | -0.3 | 25.0 |
| 1025 | 2.2 |  | 10.3 | 1026 | 1.5 | 12.4 | 1026 | 1.2 | 15.1 | 1026 | 0.8 | 17.6 | 1023 | 1.3 | 14.6 | 1023 | 0.7 | 17.0 | 1022 | 0.4 | 19.7 | 1023 | 0.1 | 24.0 |
| 1075 | 2.5 |  | 8.1 | 1076 | 1.8 | 9.8 | 1076 | 1.6 | 12 | 1076 | 1.7 | 15.5 | 1075 | 2.0 | 12.7 | 1075 | 1.1 | 14.7 | 1075 | 0.9 | 17.7 | 1075 | 0.3 | 22.3 |
| 1119 | 5.2 |  | 1.6 | 1120 | 4.8 | 1.7 | 1120 | 4.2 | 2.2 | 1120 | 3.0 | 6.2 | 1120 | 4.0 | 4.8 | 1119 | 4.3 | 4.1 | 1119 | 4.6 | 6.8 | 1120 | 2.1 | 12.7 |
| 1160 | 4.4 |  | 9.5 | 1160 | 2 | 9.3 | 1160 | 0.3 | 7.9 | 1160 | 3.4 | 4.3 | 1160 | 3.0 | 4.3 | 1160 | 4.4 | 5.9 | 1160 | 4.2 | 4.4 | 1160 | 7.2 | 2.5 |
| Tklinker (°C): |  | 1089 |  | 1097 |  |  | 1103 |  |  | 1124 |  |  | 1113 |  |  | 1111 |  |  | 1133 |  |  | 1146 |  |  |
| Tsinter (°C): |  | 1116 |  | 1118 |  |  | - |  |  | - |  |  | - |  |  | - |  |  | - |  |  | - |  |  |
| G0 – pure clay; G1 – clay+10wt.% of old sediment (Sed10); G2 - clay+20wt.% of old sediment (Sed10); G3 - clay+30wt.% of old sediment (Sed10); G5 - clay+10wt.% of new sediment (Sed1); G6 - clay+20wt.% of new sediment (Sed1); G7- clay+30wt.% of new sediment (Sed1); G8 - clay+50wt.% of new sediment (Sed1) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |