Supplementary Information

Environmental hazard of polypropylene microplastics from disposable medical masks: acute toxicity towards Daphnia magna and current knowledge on other polypropylene microplastics

Anita Jemec Kokalj1,*, Andraž Dolar1, Damjana Drobne1, Marjan Marinšek2, Matej Dolenec3, Luka Škrlep4, Gregor Strmljan4, Branka Mušič4, Andrijana Sever Škapin4

1University of Ljubljana, Biotechnical Faculty, Department of Biology, Večna pot 111, SI-1000 Ljubljana, Slovenia

2University of Ljubljana, Faculty of Chemistry and Chemical Technology, Chair of Materials and Polymer Science, Večna pot 113, SI-1000 Ljubljana, Slovenia

3University of Ljubljana, Faculty of Natural Sciences and Engineering, Department of Geology, Aškerčeva 12, SI-1000 Ljubljana, Slovenia

4Slovenian National Building and Civil Engineering Institute; Dimičeva ulica 12; SI-1000 Ljubljana, Slovenia

*Corresponding author: Anita Jemec Kokalj

Department of Biology

Biotechnical Faculty

University of Ljubljana

Večna pot 111

SI-1000 Ljubljana, Slovenia

Email: anita.jemec@bf.uni-lj.si

Fourier-transform infrared spectroscopy

Figure S1

Figure S1. Attenuated total reflection–Fourier-transform infrared spectroscopy spectra for the polypropylene standard (from the internal Slovenian National Building and Civil Engineering Institute [ZAG] database) and for the inner frontal, middle filtering and outer layers of the milled medical mask.

Gas chromatography–mass spectrometry analysis

Figures S2-S6

Figure S2. The GS-MS chromatogram of solvent (methanol).

Figure S3. The GS-MS chromatogram of procedural blank.

Figure S4. GC-MS chromatogram of the extract of the milled inner frontal layer of the face mask.

Figure S5. GC-MS chromatogram of extract of the milled middle filtering layer of the face mask.

Figure S6. GC-MS chromatogram of the extract of the milled outer blue layer of the face mask.

A review of ecotoxicity data on polypropylene microplastics

Table S1. Search keywords and the number of results obtained.  The number of relevant studies is also marked.

|  | WoS (advanced search: articles, category: Environmental Sciences | ScienceDirect (advanced search: Research articles, subject area Environmental Sciences) |
| --- | --- | --- |
| “Microplastics” and “polypropylene” | 688 (20 relevant) | 2003 (14 relevant) |
| “Microplastics” and “polypropylene” and “toxic” | 59 (7 relevant1) | 1175 (13 relevant2) |

1all the same as for the “Microplastics” and “polypropylene” WoS search, 212 of these are the same as for the “Microplastics” and “polypropylene” ScienceDirect search