Sustainable alkali-activated slag binders based on alternative activators sourced from mineral wool and glass waste

Majda Pavlin1†, Katja Konig1, Jakob Konig2, Uroš Javornik3 and Vilma Ducman1,*

1Slovenian National Building and Civil Engineering Institute (ZAG Ljubljana), Dimičeva 12, 1000 Ljubljana, Slovenia, www.zag.si

2Jožef Stefan Insitute, Jamova 39, 1000 Ljubljana

3Slovenian NMR Centre, National Institute of Chemistry, Hajdrihova 19, 1000 Ljubljana

*Corresponding author: Vilma Ducman, Slovenian National Building and Civil Engineering Institute, Dimičeva 12, 1000 Ljubljana, SLOVENIA, vilma.ducman@zag.si

Content (2 tables and 2 figures):

-	Table S1: Particle size distribution.

- 	Table S2: Si/Al ratios in AAAs and AAMs, Ca/Si ratio in AAMs and Si-O-T position

-	Figure S1: Particle size distribution.

- 	Figure S2: Pore size distribution in AAMs.

Table S1: Diameter determined by laser particle size analysis (d10, d50 and d90).

|  | SW (µm) | GW (µm) | BG (µm) | CRTG (µm) | EAFS (µm) |
| --- | --- | --- | --- | --- | --- |
| d10 | 5.67 | 5.35 | 2.01 | 1.70 | 1.25 |
| d50 | 24.91 | 19.35 | 19.47 | 18.32 | 19.30 |
| d90 | 65.92 | 62.08 | 75.80 | 78.85 | 70.93 |

Table S2: Si/Al ratios in AAAs prepared for use in the alkali activation of slag (EAFS), Si/Al and Ca/Si ratios in AAMs and the position of Si-O-T asymmetric stretching bands.

| Sample | Si/Al (in AAAs)* | Si/Al (in AAM)** | Ca/Si** | Si-O-T (cm-1) |
| --- | --- | --- | --- | --- |
| 1_BG-KOH-4h | 61.6 | 1.61 | 0.96 | 956 |
| 2_BG-KOH-24h | 60.0 | 1.79 | 0.86 | 965 |
| 3_CRTG-KOH-4h | 29.3 | 1.62 | 0.95 | 959 |
| 4_CRTG-KOH-24h | 32.4 | 1.66 | 0.93 | 940 |
| 5_GW-KOH-4h | 22.7 | 1.63 | 0.95 | 940 |
| 6_GW-KOH-24h | 29.6 | 1.72 | 0.89 | 947 |
| 7_SW-KOH-4h | 3.61 | 1.55 | 0.98 | 951 |
| 8_SW-KOH-24h | 2.81 | 1.56 | 0.99 | 940 |
| Ref_10M-KOH | / | 1.52 | 1.01 | 962 |
| Ref_K-silicate | / | 2.99 | 0.52 | 982 |

*Calculated based on concentrations measured in the AAAs.     **Calculated based on XRF and XRD data. XRD data was taken from a previous study by Češnovar et al. (34).

Figure S1: Particle size distribution of materials used for preparation of alternative activators (SW, GW, BG and CRTG) and alkali activation (EAFS).

Figure S2: Pore size distribution of the hardened binders composed of alkali-activated fly slag, after curing at 70 °C for 72 h.