Electronic Supplementary Information

Combining CaCO3 mineralisation and thermal modification for improved fungal resistance of selected wood species

Rožle Repič, Andreja Pondelak, Davor Kržišnik, Miha Humar and  Andrijana Sever Škapin

DVS analysis – beech wood

Figure S1: DVS curve for native beechwood.

Figure S2: DVS curve for TM beechwood.

Figure S3: DVS curve for mineralised beechwood.

Figure S4: DVS curve for beechwood treated with both procedures.

DVS – spruce wood

Figure S5: DVS curve for native sprucewood.

Figure S6: DVS curve for TM sprucewood.

Figure S7: DVS curve for mineralised sprucewood.

Figure S8: DVS curve for sprucewood treated with both procedures.

DVS analysis – Calcium carbonate

Figure S9: DVS curve for CaCO3 incoroprated in woods structure.

Figure 10: Samples of sprucewood before exposure to fungi (NE)(first row); samples of sprucewood after exposure to fungi .

Figure 11: Samples of beechwood before exposure to fungi(NE)(first row); samples of beech wood after exposure to fungi.

Figure 12: XRD patterns of native sprucewood (black) sprucewood mineralised by CaCO3 (blue) and sprucewood mineralised by CaCO3 sfter exposure to fungi. V-vaterite; O-calcium oxalate hydrate. 
Vaterite  CaCO3 (Card no.  00-033-0268); Calcium oxalate hydrat CaCO3  (Card no.  00-020-0233).