Supporting information

Influence of microwaves in the early stage of alkali-activation on the mechanical strength of alkali-activated materials

Barbara Horvat1,*, Majda Pavlin1, Vilma Ducman1

1Slovenian National Building and Civil Engineering Institute (ZAG Ljubljana), Dimičeva 12, 1000 Ljubljana, Slovenia, www.zag.si

*Corresponding author: Barbara Horvat, Slovenian National Building and Civil Engineering Institute, Dimičeva 12, 1000 Ljubljana, Slovenia, barbara.horvat@zag.si; Tel.: +386-40-394-270 (B.H.)

Content (3 figures and 1 table):

- Figure S1: XRD patterns of precursors.

- Figure S2: Rietveld refinement results of precursors and their long-term alkali-activated optimal mixtures.

- Figure S3: XRD patterns of precursors and their long-term alkali-activated optimal mixtures.

- Table S1: XRD mineral cards, and their chemical formulas, used for precursors and AAMs.

XRD patterns of precursors FA, SR and MK are presented in Figure S1 with an enlarged y-axis part containing an amorphous content and background (high quartz peak in MK squeezes/hides behaviour of base-line; figure S1 (b)). Peak identification is presented in Figure S3.

Figure S1. (a) XRD patterns of precursors FA, SR and MK, and (b) enlarged part ascribed to amorphous content and background coming from the apparatus.

Rietveld refinement results and their XRD patterns of precursor SR, FA and MK, used for calculations of optimal mixture designs, with the optimally irradiated and non-irradiated limit results of AAMs, are presented in Figure S2 and Figure S3, respectively.

Figure S2. Rietveld refinement of precursor FA, SR and MK, and their long-term limit results of the most optimal AAM mixtures optimally irradiated and non-irradiated.

XRD patterns of 156-days-old irradiated (1) and non-irradiated (0) FAa (irradiation for 15 s at 40%), SRa (irradiation for 20 s at 60%) and MKa (irradiation for 5 s at 60%) with precursors. With dashed lines are marked minerals that form or disappear (except for MK). Mineral cards with their chemical formulas used for precursors and AAMs are listed in Table S1.

Figure S3. XRD patterns of a long-time limit of optimally irradiated and non-irradiated AAMs with precursors.

Table S1. XRD mineral cards and their chemical formulas, which were used for solving XRD patterns of precursors and AAMs.

| Mineral name | Mineral card, reference code | Chemical formula |
| --- | --- | --- |
| FA and AAM from FA |  |  |
| Quartz | ICSD 98-008-9278 | SiO2 |
| Hematite | ICSD 98-016-1291 | Fe2O3 |
| Mullite | ICSD 98-004-3298 | Al1.83Si1.08O4.85 |
| Akermanite-Gehlenite | ICSD 98-016-0338 | Ca2Mg0.35Al1.3Si1.35O7 |
| Magnesioferrite | ICSD 98-024-0794 | Fe2MgO4 |
| Anhydrite | ICSD 98-000-1956 | CaSO4 |
| Anorthite | ICSD 98-000-0654 | Ca(AlSiO4)2 |
| Albite | ICSD 98-008-7660 | NaAlSi3O8 |
| Calcite | ICSD 98-001-8166 | CaCO3 |
| SR and AAM from SR |  |  |
| Quartz | ICSD 98-015-6198 | SiO2 |
| Hematite | ICSD 98-041-5251 | Fe2O3 |
| Magnesioferrite | ICSD 98-015-8433 | Fe2MgO4 |
| Calcite | ICSD 98-002-0179 | CaCO3 |
| Calcio-olivine | ICSD 98-000-9095 | Ca2SiO4 |
| Larnite | ICSD 98-003-9006 | Ca2SiO4 |
| Brownmillerite | ICSD 98-024-5648 | Ca2Mg0.1Al0.9FeO5 |
| Dolomite | ICSD 98-017-1521 | CaMg(CO3)2 |
| Chromite | ICSD 98-017-1112 | Cr2Fe0.32Mg0.68O4 |
| Brucite | ICSD 98-007-7086 | Mg(OH)2 |
| MK and AAM from MK |  |  |
| Quartz | ICSD 98-009-0145 | SiO2 |
| Anatase | ICSD 98-015-6838 | TiO2 |