Supporting information

Mechanical, microstructural and mineralogical evaluation of alkali-activated waste glass and stone wools

Majda Pavlin, Barbara Horvat, Ana Frankovič and Vilma Ducman*

Slovenian National Building and Civil Engineering Institute (ZAG Ljubljana), Dimičeva 12, 1000 Ljubljana, Slovenia, www.zag.si

*Corresponding author: Vilma Ducman, Slovenian National Building and Civil Engineering Institute, Dimiceva 12, 1000 Ljubljana, SLOVENIA

Content (1 figure and 2 tables):

- Figure S1: Organic binder in AAMs.

- Table S1: Mechanical properties, curing 3 days at 40 °C.

- Table S2: Mechanical properties, curing 90 days at room temperature.

Drying process

Organic binder

Figure S1: Organic binder present in AAMs made of SW or GW. Two different types of pore are seen, one that are formed as a consequence of the drying process and pores present due to the organic binder by the reaction between alkaline activator and an organic binder.

Table S1: The results of compressive and flexural strengths different alkali-activated samples of glass (GW), stone wool (SW) after 3 days of curing at 40 °C.

| Time (days) | Compressive strength (MPa) | Standard deviation (MPa) | Flexural strength (MPa) | Standard deviation (MPa) |
| --- | --- | --- | --- | --- |
| GW1 | 11.1 | 1.41 | 3.81 | 0.19 |
| GW2 | 53.1 | 4.61 | 15.8 | 2.37 |
| GW3 | 38 | 0.37 | 12.7 | 1.59 |
| GW4 | 36.9 | 4.33 | 12.0 | 0.63 |
| GW5 | 38.4 | 1.5 | 10.7 | 1.01 |
| SW1 | 24.5 | 0.72 | 9.32 | 1.72 |
| SW2 | 40.6 | 1.03 | 8.28 | 0.67 |
| SW3 | 27.2 | 1.45 | 7.79 | 0.09 |
| SW4 | 30.57 | 1.94 | 6.47 | 1.32 |
| SW5 | 31.6 | 0.65 | 9.81 | 0.39 |

Table S2: The compressive and flexural strengths of alkali-activated GW5 (a) and SW5 samples (b) measured after 1, 3, 7, 14, 28, 56 and 90 days, cured at room temperature.

- GW5

| Time (days) | Compressive strength (MPa) | Standard deviation (MPa) | Flexural strength (MPa) | Standard deviation (MPa) |
| --- | --- | --- | --- | --- |
| 1 | 0 | 0 | 0 | 0 |
| 3 | 0 | 0 | 0 | 0 |
| 7 | 6.1 | 0.63 | 2.44 | 0.50 |
| 14 | 17.4 | 0.61 | 7.25 | 1.58 |
| 28 | 32.2 | 1.11 | 9.64 | 0.78 |
| 56 | 58.2 | 2.03 | 17.6 | 3.94 |
| 90 | 76.4 | 2.75 | 27.0 | 0.90 |

- SW5

| Time (days) | Compressive strength (MPa) | Standard deviation (MPa) | Flexural strength (MPa) | Standard deviation (MPa) |
| --- | --- | --- | --- | --- |
| 1 | 0 | 0 | 0 | 0 |
| 3 | 0 | 0 | 0 | 0 |
| 7 | 9.61 | 0.2 | 2.86 | 0.0 |
| 14 | 25.5 | 1.92 | 7.82 | 2.07 |
| 28 | 34.1 | 1.62 | 8.68 | 0.14 |
| 56 | 49.7 | 2.03 | 13.3 | 0.43 |
| 90 | 55.8 | 1.61 | 13.5 | 1.00 |