Supporting information

High temperature resistant fly-ash and metakaolin-based alkali-activated foams

Katja Traven1, Mark Češnovar1,2, Srečo D. Škapin3, Vilma Ducman1

1Slovenian National Building and Civil Engineering Institute (ZAG), Dimičeva 12, 1000 Ljubljana, Slovenia

2International Postgraduate School Jožef Stefan, Jamova 39, 1000 Ljubljana, Slovenia

3Jožef Stefan Institute, Jamova 39, 1000 Ljubljana, Slovenia

*Corresponding author: Vilma Ducman, Slovenian National Building and Civil Engineering Institute, Dimičeva 12, 1000 Ljubljana, SLOVENIA

Content (1 table):

- Table S1: A list of the absolute and relative compressive strengths, σCS, (with regard to the unexposed sample, designated as R.T.), together with the densities (ρ) of all samples.

Table S1: A list of the absolute and relative compressive strengths, σCS, (with regard to the unexposed sample, designated as R.T.), together with the densities (ρ) of all samples.

|  |  | σCS (MPa) | Relative σCS (%) | ρ (g/cm3) | Relative ρ (%) |
| --- | --- | --- | --- | --- | --- |
| 1Na | R.T. | 1.24 (± 0.14) | / | 0.60 (± 0.01) | / |
|  | 600 °C | 0.57 (± 0.09) | 46.0 | 0.53 (± 0.02) | 88.3 |
|  | 800 °C | 1.88 (± 0.14) | 151.6 | 0.53 (± 0.03) | 88.3 |
|  | 1000 °C | 3.82 (± 0.40) | 308.1 | 0.55 (± 0.02) | 91.7 |
|  | 1200 °C | 56.42 (± 3.65) | 4550.0 | 1.31 (± 0.01) | 218.3 |
| 2Na | R.T. | 2.17 (± 0.27) | / | 0.59 (± 0.01) | / |
|  | 600 °C | 1.85 (± 0.10) | 85.3 | 0.56 (± 0.01) | 94.9 |
|  | 800 °C | 2.88 (± 0.29) | 132.7 | 0.57 (± 0.01) | 96.6 |
|  | 1000 °C | 4.51 (± 0.48) | 207.8 | 0.61 (± 0.02) | 103.4 |
|  | 1200 °C | 44.87 (± 8.30) | 2067.7 | 1.12 (± 0.07) | 189.8 |
| 3Na | R.T. | 2.28 (± 0.28) | / | 0.55 (± 0.01) | / |
|  | 600 °C | 1.97 (± 0.16) | 86.4 | 0.56 (± 0.01) | 101.8 |
|  | 800 °C | 2.54 (± 0.30) | 111.4 | 0.60 (± 0.03) | 109.1 |
|  | 1000 °C | 3.27 (± 0.48) | 143.4 | 0.59 (± 0.02) | 107.3 |
|  | 1200 °C | 33.36 (± 3.01) | 1463.2 | 1.14 (± 0.04) | 207.3 |
| 4Na | R.T. | 2.55 (± 0.22) | / | 0.63 (± 0.02) | / |
|  | 600 °C | 1.36 (± 0.13) | 53.3 | 0.56 (± 0.01) | 88.9 |
|  | 800 °C | 2.06 (± 0.12) | 80.8 | 0.62 (± 0.01) | 98.4 |
|  | 1000 °C | 4.57 (± 0.26) | 179.2 | 0.70 (± 0.02) | 111.1 |
|  | 1200 °C | 34.69 (± 5.72) | 1360.4 | 1.48 (± 0.14) | 234.9 |
| 1K | R.T. | 2.94 (± 0.54) | / | 0.92 (± 0.02) | / |
|  | 600 °C | 2.37 (± 0.58) | 80.6 | 0.79 (± 0.07) | 85.9 |
|  | 800 °C | 4.40 (± 1.11) | 124.5 | 0.86 (± 0.07) | 93.5 |
|  | 1000 °C | 8.86 (± 1.52) | 301.4 | 0.86 (± 0.04) | 93.5 |
|  | 1200 °C | 7.63 (± 0.86) | 259.5 | 0.95 (± 0.11) | 103.3 |
| 2K | R.T. | 3.06 (± 0.27) | / | 0.75 (± 0.04) | / |
|  | 600 °C | 2.52 (± 0.62) | 82.4 | 0.74 (± 0.08) | 98.7 |
|  | 800 °C | 2.96 (± 0.88) | 96.7 | 0.76 (± 0.09) | 101.3 |
|  | 1000 °C | 11.93 (± 1.83) | 389.9 | 0.97 (± 0.07) | 129.3 |
|  | 1200 °C | 9.63 (± 1.51) | 314.7 | 0.90 (± 0.02) | 120.0 |
| 3K | R.T. | 2.36 (± 0.12) | / | 0.76 (± 0.05) | / |
|  | 600 °C | 1.71 (± 0.71) | 72.5 | 0.72 (± 0.03) | 94.7 |
|  | 800 °C | 2.06 (± 0.28) | 87.3 | 0.69 (± 0.01) | 90.8 |
|  | 1000 °C | 3.63 (± 0.73) | 153.8 | 0.76 (± 0.02) | 100.0 |
|  | 1200 °C | 6.36 (± 1.20) | 269.5 | 0.84 (± 0.05) | 110.5 |
| 4K | R.T. | 5.12 (± 0.67) | / | 0.90 (± 0.02) | / |
|  | 600 °C | 3.53 (± 0.26) | 68.9 | 0.88 (± 0.01) | 97.8 |
|  | 800 °C | 3.40 (± 0.38) | 66.4 | 0.85 (± 0.01) | 94.4 |
|  | 1000 °C | 7.68 (± 0.97) | 150.0 | 0.96 (± 0.05) | 106.7 |
|  | 1200 °C | 14.30 (± 2.65) | 279.3 | 1.07 (± 0.05) | 118.9 |