Supplementary Table 1: Ecorr and │Z│values (raw values) for the different investigated fluoropolymer coatings and for reference without a coating (the aged bronze sample)

| Coating | FA-MS-BS |  | LbL-FA-2MS-BS |  | FA-MS |  | LbL-FA-2MS |  | Aged bronze sample |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Time | Ecorr /mV | │Z│ /kΩ cm2 | Ecorr /mV | │Z│ /kΩ cm2 | Ecorr/mV | │Z│ /kΩ cm2 | Ecorr /mV | │Z│ /kΩ cm2 | Ecorr /mV | │Z│/kΩ cm2 |
| 1 h | 34 | 1058 | 5 | 604 | 43 | 9650 | 12 | 1736 | 3 | 0.6 |
| 1 day | 137 | 1078 | 29 | 262 | 34 | 7289 | 43 | 1879 | 31 | 2.8 |
| 3 days | 93 | 777 | 38 | 116 | 37 | 6914 | 43 | 1326 | 36 | 2.8 |
| 1 week | 75 | 545 | 63 | 1728 | 41 | 20682 | 54 | 3094 | 84 | 3.8 |
| 2 weeks | 83 | 1037 | 27 | 1184 | 43 | 5170 | 70 | 8033 | 100 | 12.9 |
| 3 weeks | 116 | 1563 | 34 | 237 | 38 | 6257 | 77 | 2286 | 113 | 11.3 |
| 4 weeks | 130 | 1791 | 30 | 355 | 45 | 5621 | 64 | 1201 | 96 | 6.9 |