Electronic Supplementary Material for:

Experimental study and thermodynamic modelling of the temperature effect on the hydration of belite-ye’elimite-ferrite cements

Maruša Mrak1, 2, Frank Winnefeld3, Barbara Lothenbach3,4, Andraž Legat1, Sabina Dolenec1,*

1 Slovenian National Building and Civil Engineering Institute, Dimičeva ulica 12, 1000 Ljubljana, Slovenia

2 Jožef Stefan International Postgraduate School, Jamova cesta 39, 1000 Ljubljana, Slovenia

3 Empa, Swiss Laboratories for Materials Science and Technology, Überlandstrasse 129, 8600 Dübendorf, Switzerland

4 Norwegian University of Science and Technology (NTNU), Department of Structural Engineering, Trondheim, Norway

* Corresponding author. Tel.: +386 40 693 125. E-mail address: sabina.dolenec@zag.si

In the following Figures S1–S3, the data reported in this study are summarized, as they are already discussed in detail in the paper.

Fig. S1 X-ray diffraction patterns of cement mixtures BYF-B (a) and BYF-Y (b) at 7 days of hydration at different curing temperatures. B = belite, E = ettringite, F = ferrite, G = gypsum, Ms = monosulfate, P = perovskite, S = strätlingite, Si-Hg = siliceous hydrogarnet

Fig. S2 X-ray diffraction patterns of cement mixtures BYF-B (a) and BYF-Y (b) at 28 days of hydration at different curing temperatures. B = belite, E = ettringite, Ms = monosulfate, P = perovskite, S = strätlingite, Si-Hg = siliceous hydrogarnet

Fig. S3 Thermogravimetric analysis of cement paste BYF-B at 7 and 28 days (a and b) of hydration and cement paste BYF-Y at 7 and 28 days (c and d) of hydration. AH3 = aluminium hydroxide, C-S-H = calcium silicate hydrate, E = ettringite, G = gypsum, Ms = monosulfate, S = strätlingite, Si-Hg = siliceous hydrogarnet