Supplementary material

Diffusive reflectance spectra

Fig. S1 presents the diffusive reflectance UV-Vis spectra (R) of the a) non functionalized and b) functionalized samples.

Fig. S1: Diffuse reflectance UV-Vis spectra of a) the non-functionalized samples, b) the functionalized samples.

Mass loss of non-functionalized samples

In the Table S1 the entire mass loss of non-functionalized samples determined by thermogravimetry in the temperature range between 190 and 700 °C in first column is presented, the mass loss of CR in the second and the theoretical mass loss if all CR will be adsorbed is presented in  column 3.

Table S1: Determined mass loss of non-functionalized samples with variation in loaded CR, calculated mass loss of the CR in MS-CR, theoretical mass loss of the CR in CR-MS.

|  | sample | Mass loss (TG, 190-700 °C) / % | Mass loss of CR / % | Theoretical mass loss of CR / % |
| --- | --- | --- | --- | --- |
|  | MS | 0.54 | / | / |
|  | MS-CR1 | 1.29 | 0.75 | 0.99 |
|  | MS-CR3 | 3.32 | 2.8 | 2.9 |
|  | MS-CR5 | 5.23 | 4.7 | 4.8 |
|  | MS-CR10 | 9.49 | 8.9 | 9.1 |
|  | MS-CR35 | 25.87 | 25.3 | 25.9 |

TG-MS curves for CR, MS-CR10 and N-MS-CR10 samples

TG-MS curves for samples CR, MS-CR10 and N-MS-CR10 together with signals 18, 17, 30, 44, 58 and 64 m/z are presented in the Fig. S2.

Fig. S2: Comparison of TG-MS curves of a) CR, b ) MS-CR10 and c) N- MS-CR10 samples. For the illustrative display of the selected m/z curves followed signals were magnified: The signals 30 and 44 m/z were magnified 100 times and the signals 58 and 64 m/z 500 times.

TG-DSC curves for cresol red

The TG-DSC curves for CR sample are presented in Fig. S3.

Fig. S3: TG-DSC curves for CR.