SUPPLEMENTARY INFORMATION

COMPARING THE EFFECTS OF PRISTINE AND UV-VIS AGED MICROPLASTICS: BEHAVIOURAL RESPONSE OF MODEL TERRESTRIAL AND FRESHWATER CRUSTACEANS

Primož Zidar1, Dana Kühnel2, Andrijana Sever Škapin3,4, Tina Skalar5, Damjana Drobne1, Luka Škrlep3, Branka Mušič3, Anita Jemec Kokalj1,*

1University of Ljubljana, Biotechnical Faculty, Department of Biology, Jamnikarjeva 101, SI-1000 Ljubljana, Slovenia

2Helmholtz Centre for Environmental Research – UFZ, Permoserstr. 15, 03418 Leipzig, Germany

3Slovenian National Building and Civil Engineering Institute; Dimičeva ulica 12; SI-1000 Ljubljana, Slovenia

4Faculty of Polymer Technology—FTPO, Ozare 19, SI-2380 Slovenj Gradec, Slovenia

5University of Ljubljana, Faculty of Chemistry and Chemical Technology, Večna pot 113, SI-1000 Ljubljana, Slovenia

*corresponding author, anita.jemec@bf.uni-lj.si

Figure S1. Experimental set-up with Daphnia magna

Figure S2: Experimental set-up with woodlice Porcellio scaber.

Figure S3. Photos of particles before and after UV-VIS induced ageing. Significant changes of colour were observed for all medical mask-derived polypropylene microplastics.

Figure S4: Scanning electron microscopy images of aged and pristine microplastics from polypropylene medical mask: a-b) outer mask; c-d) middle mask, and e-f) inner mask. Black arrows point to the cracks. Images taken by Scanning electron microscope (LV-SEM) JSM-IT500LV (Jeol, Japan).

| A | B |
| --- | --- |
| C | D |
| E | F |

Figure S5: Fourier transform infrared-attenuated total reflectance (FTIR) spectra of aged and pristine (non-aged) samples: a) inner mask, b) middle mask and c) outer mask, d) tire particles, e) LDPE, and f) textile fibres. The regions containing bands discussed in the article are highlighted in grey.

Table S1. The specified area under band (SAUB) for C=O and CH2 (obtained by ATR-IR) used to calculate carbonyl index (CI) (Table 1).

| MP designation | SAUB C=O | SAUB CH2 | CI |
| --- | --- | --- | --- |
| Inner mask | 6,98 | 3,07 | 2,24 |
| Middle mask | 3,97 | 2,45 | 1,62 |
| Outer mask | 2,53 | 2,21 | 1,30 |
| Tire particles | 1,33 | 1,75 | 0,75 |
| LDPE | 0,51 | 2,55 | 0,20 |