Supplementary files: Figure S1: Electrochemical impedance spectroscopy (EIS) evaluation in 0.9% NaCl solution of reference, anodized and plasma treated Ti6Al4V alloy: a) Nyquist plot, b and c) Bode plots and d) equivalent circuits

Figure S2: Intensities of the SIMS signals of titanium oxide (TiO2-) and metallic alloy (TiAl-) from which cross section of curves the depth of oxides was determined

Table S1: Values of fitted parameters of the equivalent circuit at 1 h immersion time, Re- electrolyte resistance, CPE1- capacitive behavior of barrier layer, R1- charge transfer resistance, CPE2- capacitive behavior of defective outer layer, R2- pore resistance, Units: R [Ω cm2], CPE [Ω–1 cm–2sn]

|  | Re | CPE1 | n1 | R1 | CPE2 | n2 | R2 | Chi2 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ti6Al4V reference | 32.4 | 4.72·10-5 | 0.905 | 6.49·106 | / | / | / | 0.00021 |
| Ti6Al4V anodization | 17.2 | 1.81·10-6 | 0.913 | 38879 | 3.35·10-6 | 0.764 | 2.20·107 | 0.00039 |
| Ti6Al4V plasma | 29.0 | 2.65·10-4 | 0.99 | 35654 | 1.14·10-4 | 0.742 | 3.63·106 | 0.0037 |

Table S2: Micro-hardness measurements below the oxidized surfaces of Ti6Al4V alloy

|  | HV 0.01 |
| --- | --- |
| reference Ti6Al4V | 351  22.0 |
| Anodized Ti6Al4V | 324  17.0 |
| Plasma treated Ti6Al4V | 527  59.6 |