Manganese dioxide-coated biocarbon for integrated adsorption-photocatalytic degradation of formaldehyde in indoor conditions

Mariem Zouari 1,2,*, Silvo Hribernik 3 , Laetitia Marrot 4, Marian Tzolov 5, and David Brian DeVallance 5

1 InnoRenew CoE, Livade 6a, 6310 Izola, Slovenia

2 Faculty of mathematics, natural sciences, and information technologies; University of Primorska, Muzejski trg 2, 6000 Koper, Slovenia

3 Faculty of Electrical Engineering and Computer Science, University of Maribor, Koroška cesta 46, SI-2000 Maribor, Slovenia

4 FRISSBE, Slovenian National Building and Civil Engineering Institute (ZAG), 1000 Ljubljana, Slovenia

5 College of Science and Technology, Commonwealth University, 401 North Fairview Street, Lock Haven, PA 17745, United States

* Corresponding author: mariem.zouari@innorenew.eu

Table S1. Preparation of different BC-MnO2 samples

| Sample ID | BC, g | KMnO4, g | MnSO4, g | BC:KMnO4:MnSO4 ratio |
| --- | --- | --- | --- | --- |
| BC-MnO2-1 | 2 | 0.205 | 0.169 | 1:0.103:0.085 |
| BC-MnO2-2 | 2 | 0.316 | 0.253 | 1:0.158:0.127 |
| BC-MnO2-3 | 2 | 0.411 | 0.338 | 1:0.206:0.169 |
| BC-MnO2-4 | 2 | 0.521 | 0.422 | 1:0.261:0.211 |

Table S2. Position and ratio of D band and G band in Raman spectra of BC and BC-MnO2 samples

| Sample ID | D band position, cm-1 | G band position, cm-1 | ID/IG |
| --- | --- | --- | --- |
| BC | 1308 | 1573 | 1.22 |
| BC-MnO2-1 | 1310 | 1592 | 1.37 |
| BC-MnO2-2 | 1313 | 1590 | 1.44 |
| BC-MnO2-3 | 1307 | 1588 | 1.47 |
| BC-MnO2-4 | 1315 | 1583 | 1.41 |

Fig. S1. Distribution of the Mn elements in (a) BC-MnO2-1, (b) BC-MnO2-2, (c) BC-MnO2-3, and (d) BC-MnO2-4

Fig. S2. (a) Nitrogen adsorption–desorption isotherms obtained at 77 K and (b) total pores size distributions determined using the BJH model.

Fig. S3. (a) CO2 adsorption–desorption isotherms obtained at 273 K and (b) micropores size distributions determined using the DFT model.

Fig. S4. (a) Formaldehyde removal efficiency of BC-MnO2-3 in 24h and (b) carbon mass balance.