# Supplementary information

Table S 1 Overview of review articles (2017–2024) on the use of MSWI bottom ash as a supplementary cementitious material.

| Year | References | Contributions |  | Focus |
| --- | --- | --- | --- | --- |
| 2017 | (Verbinnen et al., 2017) | Covered case studies on the use of MSWI bottom ash as a cement replacement, with a focus on treatment methods to address chemical challenges limiting its effectiveness as an SCM. | Treatment techniques |  |
| 2018 | (Aneeta M Joseph et al., 2018) | Reviewed the application of MSWI bottom ash in Belgium as an SCM, with an emphasis on its compositional properties and methods for enhancing quality. | Compositions Treatment techniques |  |
| 2019 | (Silva et al., 2019) | Gathered findings on the leaching behavior of mixtures using MSWI bottom ash as SCM, and reviewed methods to reduce hazardous component leaching. | Treatment techniques Performances of bottom ash-blended cementitious materials (leaching behavior) |  |
| 2020 | (Cho et al., 2020) | Provided a summary of the compositional characteristics of MSWI bottom ash, as well as the fresh and mechanical properties of cementitious materials containing MSWI bottom ash. Note: This review covers only a limited selection of publications. | Compositions Performances of bottom ash-blended cementitious materials (fresh and mechanical properties) |  |
| 2021 | (Kumar & Singh, 2021) | Outlined treatments for enhancing the quality of MSWI bottom ash, focusing on reducing heavy metal leaching and improving strength and alkali-silica reaction (ASR) resistance of bottom ash-blended cementitious materials. | Treatment techniques |  |
| 2022 | (Devahi et al., 2022) | Summarized chemical and mineralogical composition data of MSWI bottom ash. Note: This review covers only a limited selection of publications. | Compositions |  |
|  | (Lu et al., 2017) | Compiled chemical composition data of MSWI bottom ash and introduced specific pre-treatment methods applied to bottom ash for improving the strength of blended cementitious materials. | Compositions Treatment techniques |  |
|  | (D. Chen et al., 2022) | Focused on the chemical composition of MSWI bottom ash, underscoring the need for pre-treatment. | Compositions |  |
| 2023 | (Snellings et al., 2023) | Provided an overview of treatment methods for MSWI bottom ash, including dry milling (followed by sieving) and wet curing of dry milled ashes (at elevated temperature or in an alkaline solution). | Treatment techniques |  |
|  | (B. Chen et al., 2023) | Conducted analysis on the compositional variety of MSWI bottom ash produced in different countries and discussed reactivity and pre-treatment techniques of MSWI bottom ash. | Compositions Reactivity Treatment techniques |  |

Table S 2 Summary of studies on the use of MSWI bottom ash as a supplementary cementitious material, including material characteristics, processing methods, mix designs, curing conditions, specimen sizes, and compressive strength.

| Origin | Particle size of collected MSWI bottom ash (μm) and industrial-scale treatment | Laboratory-scale treatments and remaining metallic aluminum (Al) content (wt.%) |  | SiO2 | CaO |  |  | Al2O3 |  | Binder |  | Water to binder ratio | Mix ratio | Curing conditions | Dimensions of tested specimen (mm) | Compressive strength at maximum ash dosage (MPa) | References |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | wt.% from XRF |  |  |  |  |  | MSWI bottom ash (Max. wt.%) | Other binders |  |  |  |  |  |  |
| Belgium | < 250 (as - received: fresh 0 -2 mm, 2 - 6 mm, 6 - 15 mm) | Ball milled + water treated+ dried (105 °C) |  | 32.1 - 56.6 |  |  | 14.47 - 22.70 | 7.77-10.4 |  | 25 | Portland cement (CEM I 52.5 N) | 0.5 | 1:3 (M) | N | 40 × 40 × 160 | 28d: decreased compared with reference mortar | (Aneeta Mary Joseph et al., 2020) |
| Belgium | < 142 D50 = 10 (as - received: 2 - 6 mm) | Ball milled + sieved Metallic Al: 0.19 |  | 43.9 |  | 18.4 |  | 10.2 |  | 25 | Portland cement (CEM I 52.5R) | 0.48 (OPC concrete) 0.46 (BA blended concrete) (superplasticizer) | C | 20 ± 2 °C, 95 ± 5 % RH | 150 × 150 × 150 | 2d and 7d: close to reference concrete 28d and 91d: higher than reference concrete | (Alderete et al., 2021) |
| Canada | Average: 9.3 | Milled Metallic Al: 0.06 |  | 28.64 |  | 22.91 |  | 14.18 |  | 20 | Portland cement | Paste (pressurized compact molding): 0.15 Concrete (dry cast): 0.35 | P C | 100% RH | Cylindrical paste: 15 (diameter) × 30 (height) Concrete: 100 × 76 × 31 | Paste: 76.5190d (88.3 % of reference OPC) Concrete: 32.0290d (18.4 % higher than reference OPC concrete) | (Zhang et al., 2021) |
| China (Mainland) | < 45 | Ball milled |  | 59.59 |  | 7.58 |  | 18.61 |  | 50 | Portland cement (PII 52.5) | N | M | 20 ± 1 °C, > 95 % RH | 40 × 40 × 160 | 10.13d, 29.228d (decreased 54.7 % and 44.5 % compared with OPC mortar) | (Li et al., 2012) |
| China (Mainland) | < 150 Average: 30 | Ball milled, Alkali treated + water washed Metallic Al: 0 |  | 25.89 |  | 32.47 |  | 6.47 |  | 20 | Portland cement | 0.484 (superplasticizer) | 1:2.75 (M) | Lime water immersion | 50 × 50 × 50 | 90d: close to reference mortar | (Liu et al., 2018) |
| China (Mainland) | < 154 Average: around 10 | Milled |  | 53.8 |  | 14.30 |  | 8.7 |  | 50 | Portland cement Class 42.5 | N | P | 20 ± 2 °C, > 90 ± 5 % RH | 40 × 40 × 160 | 28d: dramatic decrease compared with reference paste | (Yang, Ji, et al., 2018) |
| China (Mainland) | < 180 | Ball milled |  | 48.41 |  | 14.78 |  | 11.99 |  | 30 | Portland cement Class 42.5 | 0.5 | 1:3 (M) 0.5:1.86:3.78 (C) | 20 ± 2 °C, > 95 % RH | 40 × 40 × 160 | 24.428d (decreased compared with reference mortar) | (Cheng et al., 2019) |
| China (Mainland) | D50 = 10-40 (as-received: 5 - 10 mm) | Ball milled |  | 51.18 |  | 15.47 |  | 7.6 |  | 20 | Portland cement | 0.484 | 1:2.75 (M) | Ambient (23 °C) | 40 × 40 × 40 | 28d: decreased 10 - 20 % compared with OPC mortar 90d: close to OPC mortar | (Pei Tang et al., 2020) |
| China (Mainland) | D50 = 10 | Ball milled |  | 53.76 |  | 14.25 |  | 8.73 |  | 30 | Portland cement Class 42.5 | 0.5 | 1:3 (M) | 20 ± 2 °C, saturated lime water | 40 × 40 × 160 | 28d: around 40 | (Yang, Tian, et al., 2018) |
| China (Mainland) | D50 = 26.4 - 83.6 | Milling (CaCO3 was milled together with MSWI bottom ash at a mass ratio ranging of 0, 0.1, 0.2, and 0.3)) |  | 52.99 |  | 19.93 |  | 10.51 |  | 29 | Portland cement Class 42.5 | 0.3 | P | 20 ± 2 °C, 98 % RH | 40 × 40 × 160 | 28d: 29.05 - 55.84 (Paste samples were dried for 24h at ambient temperature before testing) | (Gong et al., 2022) |
| Italy | D50 = 3 | Microsphere milled (wet ground, solid/water ratio of 1:1) |  | 53.41 |  | 13.25 |  | 10.29 |  | 30 | Portland cement (CEM I 52.5 R) | 0.5 (superplasticizer) | C | 95 % RH | 100 × 100 × 100 | 64.528d (1.6 % higher than OPC concrete) 90d and 180d: higher than OPC concrete | (Bertolini et al., 2004) |
| Italy | D50 = 3.5 | wet ground (solid content in the slurry: 44 %) |  | 61.9 |  | 15.9 |  | 6.4 |  | 30 | Portland cement | 0.43 (superplasticizer) | C | 20 °C, moist curing | 100 × 100 × 100 | 87180d (around 20 % higher than OPC concrete) | (Carsana et al., 2016) |
| Then Netherlands | < 63 (as - received: < 2 mm) | Ball milled + thermally treated (550 °C, 750 °C) Metallic Al: < 0.2 |  | 35.98 |  | 19.34 |  | 9 |  | 30 | Portland cement (CEM I 52.5 R) | 0.7 | 1:3 (M) | Water immersion | 40 × 40 × 160 | 5128d (15 % reduction compared to reference mortar) | (P Tang et al., 2016) |
| The Netherlands | D50 = 39 (as - received material: < 3 mm) | Milled |  | 50.7 |  | 12.9 |  | 9 |  | 5 | Portland cement (CEM I 52.5 R and CEM I 42.5 N) | 0.5 | 1:3 (M) | N | 40 × 40 × 160 | 28d: decreased 7-11 % compared with reference mortar | (Loginova et al., 2021) |
| The Netherlands | D50 = 24 | Dry grinding + sieving+ water treatment (room temperature, 14 days, water to bottom ash ratio 0.4). The water treatment is included in the sample preparation process |  | 52.91 |  | 13.44 |  | 10.18 |  | 25 | Portland cement (CEM I 52.5 R) | 0.4 | P | 20 C, 99% RH | 20 × 20 × 20 | 90d: decreased 15 % compared with plain cement paste | (B. Chen & Ye, 2024) |
| The Netherlands | < 63 (after treatment) | Ball milling+ sieving (metallic Al content: 0.13 wt.%) |  | 39.28 |  | 22.39 |  | 10.48 |  | 30 | Portland cement (CEM I 52.5 N) | 0.5 | 1:3 (M) | 20 ± 1 °C, 95 % RH | 40 × 40 × 160 | 28d: decreased by 35.6% with 30% treated MSWI bottom ash. | (Sun et al., 2024) |
| Portugal | Average: 39 | N |  | 51.84 |  | 22.99 |  | 4.1 |  | 40 | Portland cement (CEM I 42.5 R) and coal fly ash | 0.72 (water reducer) | C | 20 ± 2 °C, 50 ± 5 % RH | 150 × 150 × 150 | Decreased compared with reference concrete | (Simões et al., 2021) |
| Slovenia | < 90 (as - received: 1 to 200 mm) | Ball milled |  | 24 |  | 39 |  | 14.8 |  | 40 | Portland cement (CEM I 42.5 R) | 0.5 | 1:3 (M) | 22 ± 2 C, 100% RH | 40 × 40 × 160 | 28d: decreased compared with OPC mortar | (Jurič et al., 2006) |
| Taiwan | < 75 | Thermal treated (1400 °C, vitrification) + Ball milled |  | 25.6 |  | 26.1 |  | 6.33 |  | 40 | Portland cement (type I) | 0.38 | P | 25 °C, > 98 % RH | Rectangular | 217d, 3828d, 5090d (decreased 42 %, 19 %, and 10 %, respectively, compared with OPC) | (Lin & Lin, 2006) |
| Taiwan | < 75 | Thermal treated (1400 °C, vitrification) + Ball milled |  | 25.6 |  | 26.1 |  | 6.3 |  | 40 | Portland cement (type I) | 0.38 | P | 25 °C, > 98 % RH | 50 × 50 × 50 | From 1d till 90d: 10 to 42 % decline compared with OPC | (Lin et al., 2008) |
| Taiwan | D90 < 21 (as - received 5 - 10 mm) | Water washed + acid washed + thermally treated (1100 °C) + ball milled |  | 38.14 (raw) 86.46 (treated) |  | 43.27 (raw) 6.14 (treated) |  | 0.19 |  | 15 vol.% (volume percentage) | 15 vol.% rice husk ash (treated at 550, 700, 900 °C) + 70 vol. % Portland cement (type I) | 0.21 (superplasticizer) | P | 25 ± 2 °C, water | 50 × 50 × 50 | 28d: 35.92-42.11 (decreased by 25.6 % to 12.8 %) | (Lo et al., 2020) |
| Thailand | < 45 D50 = 5.15 | Ball milled |  | 15.8 |  | 38.1 |  | 0.9 |  | 40 | Portland cement | 0.484 (superplasticizer) | 1:2.75 (M) | Saturated limewater | 50 × 50 × 50 | 29.37d 35.728d | (Wongsa et al., 2017) |
| US | < 90 (as - received: < 50 mm) | Ball milled Metallic Al: 0.03 % |  | N |  | N |  |  |  | 30 | Portland cement (type I) | > 0.5 | P | 21 ± 1 °C, 70 ± 3 % RH | Cylinder: 100 (diameter) × 50 (height) | 15.128d (decreased 46.6 % compared with OPC) | (Kim et al., 2016) |

N: no information

D50: Mean particle size, RH: Relative humidity, P: Paste, M: Mortar (cement: sand), C: Concrete (cement: sand: aggregate), d: day

Table S 3 Compressive strength and calculated Ash Impact Strength Index (AISI) for cement samples with and without MSWI bottom ash.

| References | 28-day Compressive strength of reference sample (MPa) | 28-day Compressive strength of sample prepared using MSWI bottom ash as supplementary cementitious material (MPa) | 28-day Ash Impact Strength Index (AISI)* | 90-day Compressive strength of reference sample (MPa) | 90-day Compressive strength of sample prepared using MSWI bottom ash as supplementary cementitious material (MPa) | 90-day Ash Impact Strength Index (AISI)* |
| --- | --- | --- | --- | --- | --- | --- |
| (Aneeta Mary Joseph et al., 2020) | 64 | 40 | 0.63 | - | - | - |
|  | 64 | 43 | 0.67 | 69 | 49.4 | 0.72 |
|  | 64 | 31 | 0.48 | - | - | - |
|  | 64 | 41 | 0.64 | - | - | - |
|  | 64 | 52.5 | 0.82 | - | - | - |
|  | 64 | 43 | 0.67 | 69 | 61 | 0.88 |
| (Alderete et al., 2021) | 52 | 40 | 0.77 | 58 | 48 | 0.83 |
| (Zhang et al., 2021) | 23 | 28 | 1.22 | 27 | 32 | 1.19 |
|  | 65 | 62 | 0.95 | 89 | 77 | 0.87 |
| (Li et al., 2012) | 53 | 46 | 0.87 | - | - | - |
|  | 53 | 43 | 0.81 | - | - | - |
|  | 53 | 39 | 0.74 | - | - | - |
|  | 53 | 29 | 0.55 | - | - | - |
| (Liu et al., 2018) | 46 | 35 | 0.76 | 53 | 52.8 | 1.00 |
| (Yang, Ji, et al., 2018) | 64 | 46 | 0.72 | - | - | - |
|  | 64 | 35 | 0.55 | - | - | - |
|  | 64 | 28 | 0.44 | - | - | - |
|  | 64 | 21 | 0.33 | - | - | - |
|  | 64 | 17 | 0.27 | - | - | - |
| (Cheng et al., 2019) | 40 | 35 | 0.88 | - | - | - |
|  | 32 | 28 | 0.88 | - | - | - |
|  | 43 | 37 | 0.86 | - | - | - |
|  | 32 | 25.5 | 0.80 | - | - | - |
|  | 43 | 34 | 0.79 | - | - | - |
|  | 32 | 25 | 0.78 | - | - | - |
|  | 40 | 31 | 0.78 | - | - | - |
|  | 43 | 32.5 | 0.76 | - | - | - |
|  | 32 | 23 | 0.72 | - | - | - |
|  | 40 | 28 | 0.70 | - | - | - |
|  | 43 | 28 | 0.65 | - | - | - |
|  | 32 | 20 | 0.63 | - | - | - |
|  | 40 | 24.5 | 0.61 | - | - | - |
|  | 43 | 26 | 0.60 | - | - | - |
|  | 40 | 23.5 | 0.59 | - | - | - |
|  | 57 | 32 | 0.56 | - | - | - |
|  | 57 | 28 | 0.49 | - | - | - |
|  | 57 | 27 | 0.47 | - | - | - |
|  | 57 | 24 | 0.42 | - | - | - |
|  | 57 | 35 | 0.61 | - | - | - |
| (Pei Tang et al., 2020) | - | - | 0.87 | - | - | 1.00 |
|  | - | - | 0.78 | - | - | 0.94 |
| (Yang, Tian, et al., 2018) | 63 | 64.5 | 1.02 | 75 | 85 | 1.13 |
| (Bertolini et al., 2004) | 65 | 70 | 1.08 | 71 | - | - |
| (Carsana et al., 2016) | 65 | 68 | 1.05 | 71 | 84 | 1.18 |
|  | 65 | 62 | 0.95 | 71 | - | - |
|  | 61 | 42 | 0.69 | - | - | - |
| (P Tang et al., 2016) | 61 | 37 | 0.61 | - | - | - |
|  | 61 | 51 | 0.84 | - | - | - |
|  | 61 | 39 | 0.64 | - | - | - |
|  | 52 | 49 | 0.94 | 58 | 56 | 0.97 |
| (Loginova et al., 2021) | 88 | 78 | 0.89 | 97 | 88 | 0.91 |
| (B. Chen & Ye, 2024) | 88 | 68 | 0.77 | 97 | 82 | 0.85 |
|  | 88 | 56 | 0.64 | 97 | 71 | 0.73 |
|  | 88 | 60 | 0.68 | 97 | - | - |
|  | 88 | 46 | 0.52 | 97 | - | - |
|  | 88 | 38 | 0.43 | 97 | - | - |
| (Sun et al., 2024) | 54 | 45 | 0.83 | - | - | - |
|  | 54 | 35 | 0.65 | - | - | - |
| (Jurič et al., 2006) | 40.6 | 43.4 | 1.07 | - | - | - |
|  | 50 | 52 | 1.04 | - | - | - |
|  | 50 | 52 | 1.04 | - | - | - |
|  | 50 | 50 | 1.00 | - | - | - |
|  | 50 | 47 | 0.94 | - | - | - |
|  | 50 | 47 | 0.94 | - | - | - |
|  | 50 | 40 | 0.80 | - | - | - |
| (Lin & Lin, 2006) | 50 | 47.5 | 0.95 | 59 | 58.5 | 0.99 |
|  | 50 | 47.5 | 0.95 | 59 | 58 | 0.98 |
|  | 50 | 40 | 0.80 | 59 | 53 | 0.90 |
| (Wongsa et al., 2017) | 46.9 | 47.7 | 1.02 | - | - | - |
|  | 46.9 | 35.7 | 0.76 | - | - | - |
| (Kim et al., 2016) | 28.3 | 26.8 | 0.95 | - | - | - |
|  | 28.3 | 15.4 | 0.54 | - | - | - |
|  | 28.3 | 15.1 | 0.53 | - | - | - |

*AISI: Ash Impact Strength Index. This index quantifies the effect of using MSWI bottom ash as SCM on the compressive strength of cement paste, mortar, or concrete. It is calculated as the ratio of the compressive strength of cement samples containing bottom ash to those without bottom ash (the reference). The index is provided for two different curing periods: 28-day and 90-day.

Table S 4 Acceptable metallic aluminum (Al) content in MSWI bottom ash for preparing blended cement pastes, mortars, and concrete, with additional information on the water-to-binder ratio, replacement level, and 28-day Ash Impact Strength Index

| Applications |  | Paste |  |  | Mortar |  |  | Concrete |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Acceptable metallic Al content (wt.%) in MSWI bottom ash |  | 0.02 | 0.13 |  | 0 | <0.2 |  | 0.06 | 0.19 |
| Water to binder (w/b) ratio |  | 0.4 | 0.5 |  | 0.484 | 0.7 |  | 0.35 | 0.46 |
| Replacement level of MSWI bottom ash (%) |  | 25 | 25 |  | 20 | 30 |  | 20 | 25 |
| 28-day Ash Impact Strength Index (AISI) |  | 0.77 | 0.65 |  | 0.76 | 0.84 |  | 1.22 | 0.77 |
| Cement type |  | CEM I 52.5R |  |  | Portland cement | CEM I 52.5R |  | Portland cement | CEM I 52.5R |
| References |  | (B. Chen & Ye, 2024) | (B. Chen et al., 2024) |  | (Liu et al., 2018) | (P Tang et al., 2016) |  | (Zhang et al., 2021) | (Alderete et al., 2021) |

Table S 5 Summary of upper limit thresholds in regulatory standards used to evaluate the toxicity of MSWI bottom ash-blended cement pastes, mortars, and concrete.

| Regions | China (Mainland) | Taiwan | USA | Singapore | The Netherlands |  |  | Slovenia | Belgium | Austria | Denmark |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Standard | GB5085.3-2007(Ministry of Ecology and Environment of the People’s Republic of China, 2007) | EPA 2018 b (Ministry of Environment, 2018) | CFR-261.24 (Federal U.S. Environmental Protection Agency, 2024) | LEACH.STD (0399) (Singapore National Environment Agency, 1988) | Soil Quality Decree, 2022 (Ministry of Infrastructure and Water Management, 2022) |  |  | Decree on waste, 2022 (Republic of Slovenia, 2022) | Vlarema 9, the Belgian Official Gazette (Vlaamse overheid, 2024) | Recycling-Built Construction Ordinance (Republic of Austria, 2024) | Statutory Order no. 1672/2016 (Kingdom of Denmark, 2016) |
| Scope of application | Solid waste | Recycled aggregates | Solid waste (except manufactured gas plant waste) | Industrial wastes for landfill disposal | Building materials |  |  | For all waste, unless otherwise specified by a special regulation for an individual type of waste or an individual waste stream | Criteria for raw materials intended for use as building materials | Parameters and limit values for aggregates for unbound as well as for hydraulically or bituminous applications | Limit values and conditions of application of bottom ash gravel for backfilling and road construction purpose |
| Regulatory value | Maximum Concentration （mg/L) |  |  |  | Upper limit value |  |  | Upper limit value (mg/kg dry solid) | Upper limit value (mg/kg dry solid) | Upper limit value (mg/kg dry solid), class U-A | Upper limit value (mg/kg dry solid), Category 3 |
|  |  |  |  |  | Unshaped material (mg/kg dry solid) |  | Monolithic material (mg/m2) | In the area without protection regime according to the regulations of the waters |  | Parameters and limit values for aggregates for unbound as well as for hydraulically or bituminous applications |  |
| Antimony (Sb) | - | - | - | - | 0.32 | 8.7 |  | - | 1 |  |  |
| Arsenic (As) | 5 | 0.4 | 5 | 5 | 0.9 | 260 |  | 0.1 | 0.8 |  | 0.10 |
| Barium (Ba) | 100 | 10 | 100 | 100 | 22 | 15000 |  | 20 | 20 |  | 8.0 |
| Cadmium (Cd) | 1 | 0.8 | 1 | 1 | 0.04 | 3.8 |  | 0.025 | 0.03 |  | 0.080 |
| Chromium (Cr) | 15 | 4 | 5 | 5 | 0.63 | 120 |  | 0.5 (total Cr), 0.1 Cr(VI) | 2.6 | 0.6 | 1.0 |
| Cobalt (Co) | - | - | - | - | 0.54 | 60 |  | 0.03 | 0.5 |  |  |
| Copper (Cu) | 100 | 12 | - | 100 | 0.9 | 98 |  | 0.5 | 0.8 | 1.0 | 4.0 |
| Mercury (Hg) | - | 0.016 | 0.2 | 0.2 | 0.02 | 1.4 |  | 0.005 | 0.02 |  | 0.002 |
| Lead (Pb) | 5 | 4 | 5 | 5 | 2.3 | 400 |  | 0.5 | 1.3 |  | 0.20 |
| Molybdenum (Mo) | - | - | - | - | 1 | 144 |  | 0.5 | 55 |  |  |
| Nickel (Ni) | 5 | - | - | 5 | 0.44 | 81 |  | 0.4 | 0.75 | 0.4 | 0.14 |
| Selenium (Se) | - | 0.8 | 1 | 1 | 0.15 | 4.8 |  | 0.6 | 2 |  | 0.060 |
| Tin (Sn) | - | - | - | - | 0.4 | 50 |  | - | 1 |  |  |
| Vanadium (V) | - | - | - | - | 1.8 | 320 |  | - | 2.5 |  |  |
| Zinc (Zn) | 100 | - | - | 100 | 4.5 | 800 |  | 2 | 2.8 |  | 3.0 |
| Fluoride (F) | - | - | - | 150 | 55 | 2500 |  | 10 | 55 |  |  |
| Chloride (Cl) | - | - | - | - | 616 | 110000 |  | 800 | 1000 | 800 | 6000 |
| Sulfate (SO42−) | - | - | - | - | 2430 | 165000 |  | 2500 | 2200 | 2500 | 8000 |
| Bromide (Br)) | - | - | - | - |  | 670 |  | - | 20 |  |  |
| Iron (Fe) | - | - | - | 100 | - | - |  |  |  |  |  |
| Silver (Ag) | - | - | 5 | 5 | - | - |  |  |  |  |  |
| Cyanide (CN) | - | - | - | 10 | - | - |  |  |  |  |  |
| Manganese (Mn) | - | - | - | 50 | - | - |  |  |  |  | 2.0 |

References

Alderete, N. M., Joseph, A. M., den Heede, P. Van, Matthys, S., & Belie, N. De. (2021). Effective and sustainable use of municipal solid waste incineration bottom ash in concrete regarding strength and durability. Resources, Conservation and Recycling, 167. https://doi.org/10.1016/j.resconrec.2020.105356

Bertolini, L., Carsana, M., Cassago, D., Curzio, A. Q., & Collepardi, M. (2004). MSWI ashes as mineral additions in concrete. Cement and Concrete Research, 34(10), 1899–1906. https://doi.org/10.1016/j.cemconres.2004.02.001

Carsana, M., Gastaldi, M., Lollini, F., Redaelli, E., & Bertolini, L. (2016). Improving durability of reinforced concrete structures by recycling wet-ground MSWI bottom ash. Materials and Corrosion, 67(6), 573–582. https://doi.org/10.1002/maco.201608881

Chen, B., Chen, J., de Mendonça Filho, F. F., Sun, Y., van Zijl, M. B., Copuroglu, O., & Ye, G. (2024). Characterization and mechanical removal of metallic aluminum (Al) embedded in weathered municipal solid waste incineration (MSWI) bottom ash for application as supplementary cementitious material. Waste Management, 176, 128–139. https://doi.org/10.1016/j.wasman.2024.01.031

Chen, B., Perumal, P., Illikainen, M., & Ye, G. (2023). A review on the utilization of municipal solid waste incineration (MSWI) bottom ash as a mineral resource for construction materials. Journal of Building Engineering, 106386. https://doi.org/https://doi.org/10.1016/j.jobe.2023.106386

Chen, B., & Ye, G. (2024). The role of water-treated municipal solid waste incineration (MSWI) bottom ash in microstructure formation and strength development of blended cement pastes. Cement and Concrete Research, 178, 107440. https://doi.org/https://doi.org/10.1016/j.cemconres.2024.107440

Chen, D., Zhang, Y., Xu, Y., Nie, Q., Yang, Z., Sheng, W., & Qian, G. (2022). Municipal solid waste incineration residues recycled for typical construction materials—a review. RSC Advances, 12(10), 6279–6291.

Cheng, Y., Dong, Y., Diao, J., Zhang, G., Chen, C., & Wu, D. (2019). MSWI bottom ash application to resist sulfate attack on concrete. Applied Sciences (Switzerland), 9(23). https://doi.org/10.3390/app9235091

Cho, B. H., Nam, B. H., An, J., & Youn, H. (2020). Municipal Solid Waste Incineration (MSWI) Ashes as Construction Materials—A Review. Materials, 13(14). https://doi.org/10.3390/ma13143143

Devahi, P., Rathod, D., & Muthukkumaran, K. (2022). Building material synthesization using municipal solid waste incineration ash: A state-of-the-art review. Environmental Technology Reviews, 11(1), 33–48. https://doi.org/10.1080/21622515.2021.2024890

Federal U.S. Environmental Protection Agency. (2024). 40 CFR 261.24: Toxicity characteristic. https://www.ecfr.gov/current/title-40/chapter-I/subchapter-I/part-261/subpart-C/section-261.24

Gong, J., Yu, L., Li, Z., & Shi, X. (2022). Mechanical activation improves reactivity and reduces leaching of municipal solid waste incineration (MSWI) bottom ash in cement hydration system. Journal of Cleaner Production, 363, 132533. https://doi.org/10.1016/j.jclepro.2022.132533

Joseph, Aneeta M, Snellings, R., Van den Heede, P., Matthys, S., & De Belie, N. (2018). The use of municipal solidwaste incineration ash in various building materials: A Belgian point of view. Materials, 11(1). https://doi.org/10.3390/ma11010141

Joseph, Aneeta Mary, Snellings, R., Nielsen, P., Matthys, S., & Belie, N. De. (2020). Pre-treatment and utilisation of municipal solid waste incineration bottom ashes towards a circular economy. Construction and Building Materials, 260, 120485. https://doi.org/10.1016/j.conbuildmat.2020.120485

Jurič, B., Hanžič, L., Ilić, R., & Samec, N. (2006). Utilization of municipal solid waste bottom ash and recycled aggregate in concrete. Waste Management, 26(12), 1436–1442. https://doi.org/10.1016/j.wasman.2005.10.016

Kim, J., An, J., Nam, B. H., & Tasneem, K. M. (2016). Investigation on the side effects of municipal solid waste incineration ashes when used as mineral addition in cement-based material. Road Materials and Pavement Design, 17(2), 345–364. https://doi.org/10.1080/14680629.2015.1083463

Kingdom of Denmark. (2016). BEK nr 1672 af 15/12/2016. Bekendtgørelse om anvendelse af restprodukter, jord og sorteret bygge- oganlægsaffald, Denmark.

Kumar, S., & Singh, D. (2021). Municipal solid waste incineration bottom ash: a competent raw material with new possibilities. Innovative Infrastructure Solutions, 6, 1–15.

Li, X. G., Lv, Y., Ma, B. G., Chen, Q. Bin, Yin, X. B., & Jian, S. W. (2012). Utilization of municipal solid waste incineration bottom ash in blended cement. Journal of Cleaner Production, 32, 96–100. https://doi.org/10.1016/j.jclepro.2012.03.038

Lin, K. L., Chang, W. C., & Lin, D. F. (2008). Pozzolanic characteristics of pulverized incinerator bottom ash slag. Construction and Building Materials, 22(3), 324–329. https://doi.org/10.1016/j.conbuildmat.2006.08.012

Lin, K. L., & Lin, D. F. (2006). Hydration characteristics of municipal solid waste incinerator bottom ash slag as a pozzolanic material for use in cement. Cement and Concrete Composites, 28(9), 817–823. https://doi.org/10.1016/j.cemconcomp.2006.03.003

Liu, Y., Sidhu, K. S., Chen, Z., & Yang, E. H. (2018). Alkali-treated incineration bottom ash as supplementary cementitious materials. Construction and Building Materials, 179, 371–378. https://doi.org/10.1016/j.conbuildmat.2018.05.231

Lo, F. C., Lo, S. L., & Lee, M. G. (2020). Effect of partially replacing ordinary Portland cement with municipal solid waste incinerator ashes and rice husk ashes on pervious concrete quality. Environmental Science and Pollution Research, 27(19), 23742–23760. https://doi.org/10.1007/S11356-020-08796-Z

Loginova, E., Schollbach, K., Proskurnin, M., & Brouwers, H. J. H. (2021). Municipal solid waste incineration bottom ash fines: Transformation into a minor additional constituent for cements. Resources, Conservation and Recycling, 166. https://doi.org/10.1016/j.resconrec.2020.105354

Lu, J.-W., Zhang, S., Hai, J., & Lei, M. (2017). Status and perspectives of municipal solid waste incineration in China: A comparison with developed regions. Waste Management, 69, 170–186. https://doi.org/https://doi.org/10.1016/j.wasman.2017.04.014

Ministry of Ecology and Environment of the People’s Republic of China. (2007). Solid waste-Extraction procedure for leaching toxicity-Sulphuric acid & nitric acid method, HJ/T 299.

Ministry of Environment. (2018). Taiwan EPA Laws and Regulation Retrieving System (2018b).

Ministry of Infrastructure and Water Management. (2022). Soil Quality Decree. https://wetten.overheid.nl/BWBR0047808/2025-05-21#BijlageA

Republic of Austria. (2024). Recycling-Baustoffverordnung. Federal Legal Information System (RIS).

Republic of Slovenia. (2022). Decree on Waste (Nos. 37/15). Official Gazette of Republic Slovenia.

Silva, R. V, de Brito, J., Lynn, C. J., & Dhir, R. K. (2019). Environmental impacts of the use of bottom ashes from municipal solid waste incineration: A review. Resources, Conservation and Recycling, 140, 23–35. https://doi.org/https://doi.org/10.1016/j.resconrec.2018.09.011

Simões, B., da Silva, P. R., Silva, R. V, Avila, Y., & Forero, J. A. (2021). Ternary mixes of self-compacting concrete with fly ash and municipal solid waste incinerator bottom ash. Applied Sciences (Switzerland), 11(1), 1–17. https://doi.org/10.3390/app11010107

Singapore National Environment Agency. (1988). Leaching Test - Recommended Acceptance Criteria for Suitability of Industrial Wastes for Landfill Disposal. https://www.nea.gov.sg/docs/default-source/e-services-forms-docs/licences-permits-building-plan-clearances/leaching-test.pdf

Snellings, R., Suraneni, P., & Skibsted, J. (2023). Future and emerging supplementary cementitious materials. Cement and Concrete Research, 171, 107199. https://doi.org/https://doi.org/10.1016/j.cemconres.2023.107199

Sun, Y., Chen, B., Zhang, S., Blom, K., Luković, M., & Ye, G. (2024). Characterization, pre-treatment, and potential applications of fine MSWI bottom ash as a supplementary cementitious material. Construction and Building Materials, 421, 135769. https://doi.org/https://doi.org/10.1016/j.conbuildmat.2024.135769

Tang, P, Florea, M. V. A., Spiesz, P., & Brouwers, H. J. H. (2016). Application of thermally activated municipal solid waste incineration (MSWI) bottom ash fines as binder substitute. Cement and Concrete Composites, 70, 194–205. https://doi.org/10.1016/j.cemconcomp.2016.03.015

Tang, Pei, Chen, W., Xuan, D., Zuo, Y., & Poon, C. S. (2020). Investigation of cementitious properties of different constituents in municipal solid waste incineration bottom ash as supplementary cementitious materials. Journal of Cleaner Production, 258. https://doi.org/10.1016/j.jclepro.2020.120675

Verbinnen, B., Billen, P., Caneghem, J. Van, & Vandecasteele, C. (2017). Recycling of MSWI Bottom Ash: A Review of Chemical Barriers, Engineering Applications and Treatment Technologies. Waste and Biomass Valorization, 8(5), 1453–1466. https://doi.org/10.1007/s12649-016-9704-0

Vlaamse overheid. (2024). Vlarema 9 wijzigingen voor grondstofverklaringen (9th amendm). Belgisch Staatsblad.

Wongsa, A., Boonserm, K., Waisurasingha, C., Sata, V., & Chindaprasirt, P. (2017). Use of municipal solid waste incinerator (MSWI) bottom ash in high calcium fly ash geopolymer matrix. Journal of Cleaner Production, 148, 49–59. https://doi.org/10.1016/j.jclepro.2017.01.147

Yang, Z., Ji, R., Liu, L., Wang, X., & Zhang, Z. (2018). Recycling of municipal solid waste incineration by-product for cement composites preparation. Construction and Building Materials, 162, 794–801. https://doi.org/10.1016/j.conbuildmat.2017.12.081

Yang, Z., Tian, S., Liu, L., Wang, X., & Zhang, Z. (2018). Recycling ground MSWI bottom ash in cement composites: Long-term environmental impacts. Waste Management, 78, 841–848. https://doi.org/10.1016/j.wasman.2018.07.002

Zhang, S., Ghouleh, Z., He, Z., Hu, L., & Shao, Y. (2021). Use of municipal solid waste incineration bottom ash as a supplementary cementitious material in dry-cast concrete. Construction and Building Materials, 266. https://doi.org/10.1016/j.conbuildmat.2020.120890